## Slide 1: Experiences as a user of neutron diffraction

## Slide 2: Molecular magnetism
MJ = -J
MJ = J
    Direction of largest susceptibility  magnetic easy axis

## Slide 3: The use of neutrons in mm
H
Rotation angle
Susceptibility
Chart: 
Qian et al. Chem. Sci. 2015, 6, 4587-4593
Problem: This only works for triclinic crystals!

## Slide 4: The use of neutrons in mm

## Slide 5: Modelling the diffraction
  Magnetic structure factor
  Site susceptibility
  Resulting magnetic structure factor
Gukasov, A. & Brown, P.J. J. Phys. Condens. Matter 2002, 14, 8831

## Slide 6: Results from pol neutron diff
2 | 
a | 11.0343(3)
b | 12.2286(3)
c | 17.5339(5)
α | 77.103(5)▫
β | 85.701(6)▫
γ | 69.694(5)▫
a | 11.0343(3)
b | 12.2286(3)
c | 17.5339(5)
α | 77.103(5)▫
β | 85.701(6)▫
γ | 69.694(5)▫
1 | 
a | 13.2248(5)
b | 22.1323(6)
c | 16.0555(6)
α | 90▫
β | 109.646(8)
γ | 90▫
a | 13.2248(5)
b | 22.1323(6)
c | 16.0555(6)
α | 90▫
β | 109.646(8)
γ | 90▫
Klahnet al., Chem. Eur. J., 10.1002/chem.201803300 (accepted)

## Slide 7: Workflow – susceptibility refinement
# of data points (filename) | O1
Searchus (3dspots-tot.dat) | 1828
Purgealu (3dspots.dat) | 643
Indexus (indexus.lis) | 130
Intfratious (fratio.dat) | 281
Arrnge (rmoy.qsf) | 167
Purgerfli (rmoy.2si) | 36
Extcal2009 (rfl.ext) | 36
user actions

## Slide 8: Workflow – susceptibility refinement
  Two starting files containing information
    cry-file (structural information and program instructions)
    Raw detector data
Total # of files | 40
Files edited | 8
Other files | 30
Original information
Unedited files
Edited files

## Slide 9: Workflow – susceptibility refinement
Notes: It’s easy to get lost

## Slide 10: Workflow improvements

## Slide 11: conclusions
  Susceptibility refinements were largely able to be automated
  Less need for manual steps leaves
  more time for science
  ”If you do something more than 3 times,
  write a function for it”

## Slide 12: aknowledgements
  Chen Gao (AU)
  Jacob Overgaard (AU)
  Shang-Da Jiang (PKU)
  Beatrice Gillon (LLB)
  Arsen Gukasov (LLB)
  Xavier Fabreges (LLB)
  Ross O. Piltz (ANSTO)