## Slide 1
Uwe Filges
Laboratory for scientific Developments and novel Materials (LDM)
Paul Scherrer Institut
Development of New Shielding Materials
and
ESTIA - Simulations

## Slide 2: Needs at PSI/ESS - ESTIA

## Slide 3
Needs at PSI/SINQ – Upgrade AMOR
Upgraded AMOR – SELENE Type guide
Vaccum Housing of Selene guide system
inside vacuum housing 32 shielding blocks are positioned
must be high precision and non-magnetic (polarized beam)
shielding through neutron guide bunker must be very
compact because of space limitation (performance),
use of non-magnetic heavy concrete is foreseen
Bunker wall

## Slide 4: New high-precision Shielding Material – Mineral Cast
Partner: RAMPF Machine Systems GmbH & Co. KG
Mineral cast is used as the base of high-precision machines
Epument
Epustone
Epustone has the mechanical properties of granite – interesting for our ESTIA project
Epument has good shielding properties like concrete – high hydrogen content – SINQ Upgrade (AMOR)
First test series (14 compositions) in the BOA neutron field were done (activation, attenuation for diff. E)
Optimisation: add a thermal neutron absorber (B4C) in the composition.

## Slide 5: High dencity concrete
non-magnetic material -> polarized beamlines
high content of boron
high dencity material for compact shielding (> 5 g/cm3)
Partner: SACAC AG Switzerland
Characterisation on BOA and ICON Beamline at SINQ (both beamlines have fast neutrons)
Requirement
ICON beamline
measured fast neutron spectrum

## Slide 6: Measurements by Extended BSS System
PSI/BSS – System can measure neutrons up to 6 GeV

## Slide 7: Mineral Cast Samples
14 different mineral cast samples were investigated.
Epument 130 and Epument 145 are comparible to concrete
Epustone 161 is specially made as a replacement for granite
Epument is usually without Boron (test samples have 1 and 3 % B4C)
EFA (ash) is a problem because C-60 is included

## Slide 8: Mineral Cast Measurements
Best samples are: without ash and a high B4C (5%) content -> sample 6 and 9
Next Step in 2018: increasing hydrogen in sample 6 (will be measured in July 2018)
Chart: Activation and decay - Dose rate in muSv/h
| s1 | s1 | s2 | s3 | s4 | s4 | s4 | s5 | s6 | s7 | s8 | s12 | s13 | s14
 | 5.7 | 6.7 | 3.7 | 1.7 | 3.7 | 4.2 | 4.7 | 1.2 | 0.8 | 13.7 | 10.7 | 2.7 | 0.4 | 0.4
2 mins later | 3.2 | 3.7 | 2.2 | 0.5 | 2.2 | 1.7 | 0.7 | 0.7 | 0.5 | 10.7 | 6.7 | 1.7 | 0.15 | 0.1

## Slide 9: Vacuum tests
EPUMENT 130/3 – Gas Treatment
Only for high vacuum environment mineral cast shows a delayed behaviour, but neutron guides require only 1E-3 mbar
without sample

## Slide 10: Heavy Concrete Measurements
7 different concrete compositions were tested
non-magnetic / magnetic samples for different applications
Sample 1: special efforts - stainless steel balls with different sizes and thermal treatment
In addition Sample 1 includes as mineral Baryte – very good gamma shielding material
Comparison: normal concrete: < 0.13 cm-1

## Slide 11: Heavy concrete Measurements
Incoming spectrum at ICON beamline
Attenuation for the fast Neutrons
Sample with strong steel collimator (1m)
Background
shielding was needed
12 inch sphere

## Slide 12: Comparison 1 – Standard mineral cast
Thermal neutron transmission
Fast neutron transmission
Activation decay (irradiation time 10 sec)
Granite includes Thorium!
Mineral cast is better as
standard concrete or granite
12 inch sphere
bare counter

## Slide 13
Comparison 2 – Borated mineral cast – Composition 6
Thermal neutron transmission
Epithermal neutron transmission
Fast neutron transmission
Mineral cast acts like
heavy concrete !!!
12 inch sphere
bare counter
3.5 inch sphere

## Slide 14: Additional Samples
Improving shielding properties -> increase hydrogene
Improving vacuum properties -> reducing wax for making the samples
Check of mechanical properties
N1: plus 1 % more hydrogene (added over binder)
N2: plus 2 % more hydrogene (added over binder)
N3: plus 3 % more hydrogene (added over binder)
N4: new high-precision concrete with 3% B4C

## Slide 15: 4. 3.5”, transmission of 5 samples (Epi-thermal)
sample | linear attenuation coefficiency [mm-1]
no.6 | 0.0393
N1 | 0.0409
N2 | 0.0412
N3 | 0.0423
N4 | 0.0333
3.5” – has broad sensitivity in epithermal, the peak is at 10keV
Best sample is N3

## Slide 16: 5. 12”, transmission of 5 samples (Fast neutrons)
sample | linear attenuation coefficiency [mm-1]
no.6 | 0.0135
N1 | 0.0139
N2 | 0.0138
N3 | 0.0141
N4 | 0.0128
12” – sensitivity peak is at 4 MeV
Best sample is N3

## Slide 17: 6. Activation with thermal neutrons
Conclusion:
N1, N2, and N3 have the same activation level as #6. N4 has a lower activation level, but shielding performance is low.

## Slide 18
Field Test with BSS system
Small reactor facility (2 W) with very well-known
configuration
A
B
detailed MCNP model exists
at position A the fast neutron spectrum was measured
by another group (proton recoil method)
Field test was in April 2018
Verification of the known n-spectrum
Measurement an un-known n-spectrum (Pos. B)
AKR reactor at Dresden University

## Slide 19
1. High intensity beam
 The flux is ~ 102 to 103 times higher than “background” field.
 Low-efficiency detector (10-2) is available now.
2. Discriminate the “back ground” neutrons from the beam
 The shielding box (which has a lamella structure) is built and will be
tested in September 2018 at BOA.
The ideal design will be investigated.
3. Partial illumination of spheres (special response functions)
B-Al
BPE
Steel
Extension for “In-beam” measurement

## Slide 20
Bunker Components – Detailed Simulations

## Slide 21
Re-design of the MCNPX model (includes the geometry from CATIA)
ESTIA - NBOA

## Slide 22
Collimator Simulations

## Slide 23
n - Dose Rates
Det.6
Det.7
Det.8
Det.6 – 40 muSv/h
Det.7 – 85 muSv/h !!
Det. 8 – 0.2 muSv/h

## Slide 24
Thank you for your attention.