## Slide 1
Status of CiADS
Yuan He
On behalf of China ADS Groups
Institute of Modern Physics, CAS
Supported by
“Strategic Priority Research Program” of the Chinese Academy of Sciences, Future Advance Fission Energy-ADS
Mega scientific project: China Initiative Accelerator Driven System

## Slide 2: Outlines
Background of Accelerator Driven System
Design Status of CiADS
Progress of Prototypes
  Accelerator, Target and Reactor
  Material SIMP
  New Approach of Fuel Recycle
Sammary

## Slide 3: Strategy and Status of NP in China
Current status of China (including Taiwan, China) nuclear power (by the end of 2018)
  46 nuclear power reactors in operation, 42.858 GWe (3th , total 452 and 399.354 TWe in the world)
  Produced electricity: 286.5 TW.h, 4.22%
  11 reactors under construction, 10.982 GWe, (1st , total 54 in the world)
The development plan of NP in China (2014-2020)
  By 2020, the installed nuclear capacity will be 58 GWe, and 30 GWe are under construction
Nuclear energy is an inevitable strategic option to meet China energy demand in the future
  China is the largest energy consumer and Greenhouse Gas source.
  She has claimed that the CO2 emissions will reach the peak before 2030 on Paris Climate Agreement.
Data from IAEA/PRIS, update on 2019-05-18
Notes:     almost same scale of the total capacity in the world todays!

## Slide 4: One of Solution of Sustainable Development
Nuclear waste is not only the issue of sustainable, but also the long-term supply.
“The ADS has the advantage that it can burn pure minor actinides while avoiding a deterioration of the core safety characteristics.”
⎯ ADS and FR in Advanced Nuclear Fuel Cycles – A Comparative Study, NEA/OECD, 2002

## Slide 5: Sustainable Perspective of NP
Radiotoxicity Reduction  Transmutation
**Fuel < 100 y (Supply 1000GWe);
Waste Radiotoxicity>100000 y
**Fuel ~10000 y; Waste Radiotoxicity<500 y
High Resource Utilization  Breeding
Other than P&T, high radioactive elements, like Minor Actinide, will not be Partitioned but burned in ADS Buner.
ADANES Concept

## Slide 6: ADS/ADANES Roadmap in China
Inject I
Inject II
2014
~2.5 MeV
&10mA
2016
~25 MeV
&~10mA
<2030
~1.0 GeV
&<15mA
~203x
~1.0 GeV
&>15mA
10 MWt
>500 MWt
≥1 GWt
10 MeV
￥1.78 B
Phase I
2011--2016
Phase II
2018--2024
Key Tech. R&D : Acc., Target, Blanket… Prototypes
Initial Facility
Demo. Facility
Phase III
Phase IV
Indust. Facility
2024
~500 MeV
&5~10mA
“strategic Priority Research Program” of the Chinese Academy of Sciences
CiADS

## Slide 7: Outlines
Background of Accelerator Driven System
Design Status of CiADS
Progress of Prototypes
  Accelerator, Target and Reactor
  Material SIMP
  New Approach of Fuel Recycle
Sammary

## Slide 8: CiADS Project (2018-2025)
Approved in Dec. 2015
Leading institute: IMP
Budget: ~4 B CNY (Gov. + Corp.)
Location: Huizhou, Guangdong Prov.
Partners: CIAE, CGN, IHEP, etc.
Ground broke in August 2018
Earthwork will be finished by the end of the year
CiADS & HIAF

## Slide 9: Layout of CiADS
③
④
⑦
Design Particle | proton
Energy | 500 MeV
Beam current | 5 mA
Beam power | 2.5 MW
Operation mode | CW&Pulse
Reactor power | 10 MWt (incl. beam)
Cryogenic | 2 K

## Slide 10: Reliability Requirements of ADS
Whitepaper:“Accelerator and Target Technology for Accelerator Driven Transmutation and Energy Production ”2010
green “ready”
yellow “may be ready, but demonstration or further analysis is required”
Red “more development is required”
MYRRHA:
Beam-trip-duration tolerance is 3 s.
< 3 s, rapid recovery
> 3 s, <10/3months
MTBF 250 hours
© Springer International Publishing Switzerland 2016 J.-P. Revol et al. (eds.), Thorium Energy for the World, DOI 10.1007/978-3-319-26542-1_13
CiADS:
Beam-trip-duration tolerance is 10 s.
< 10 s, rapid recovery
10 s ~ 5 min, <2500 /year
> 5 min, < 50 /year

## Slide 11: Terminals planned of CiADS
T2：liquid metal target, high-power neutron source
T4：LBE sub-critical reactor
~10 MW
T3：granular target exp. 2.5 MW licenses
T1：dump, low-power exp. , ……
T5:ISOL target
Energy: 500 MeV (upgrading to 1.5GeV)
design current：10 mA
beam loss：1W/m
modes：pulse&CW（Hus gap for reactor）
energy stability：±1%@100ms
current stability：±2%@100ms
position stability：±1mm
profile stability：±1mm
T1: low power dump 50 kW; accelerator study; nuclear physics
T2: liquid metal target 250 kW ~ MW; material irradiation,
T3: granular target 100 kW ~ MW; target study
T4: 10 MW fast reactor, LBE target, Keff 0.75~0.97; demo of ADS
T5: upgrade ISOL target: iLinac of HIAF is post-acc, to 100 MeV/u

## Slide 12: Commissioning Plan of CiADS
  Characteristic: The first nuclear experimental facility for ADS principle verification of the world researches on the integration, coupling operation, transmutation and design verification with the accelerator, target and reactor system.
  Requirement： Feasibility + Flexibility
    Key technology study CiADS system integration
    Operation plan study Reliability and stability operation
  Transmutation and material research：
    Metamorphic neutrons and principle experiments of secondary lanthanides ；
    Material irradiation, etc. ；
    Experimental study on ADS fuel performance and transmutation samples ；
  Design and verification:
    Future ADS system design software development and verification
    Database and verification
    Coupling characteristics study Gradually achieve low power to high power coupling

## Slide 13: Design of SC section
 | HWR010 | HWR019 | Spoke042 | Ellip062 | Ellip082
f（MHz） | 162.5 | 162.5 | 325 | 650 | 650
βopt | 0.10 | 0.19 | 0.42 | 0.62 | 0.82
Number of cells | 2cell | 2cell | 3cell | 6cell | 5cell
Epeak(MV/m) | 26/30 | 28/33 | 28/33 | 28/33 | 28/33
Num of cavities | 9 | 24 | 40 | 40 | 24
Focusing elements | SC sol | SC sol | SC sol | triplet | doublet
Num of magnets | 9 | 24 | 20 | 10 | 6
Magnet field(T) | 7.5 | 7.5 | 7.5 | 0.9 | 0.9
Length of CM(m) | 6 | 6 | 6 | 6 | 6
Num of CMs | 1 | 4 | 10 | 10 | 6
Beam
dump
Physics ：phase advance <90; smoothness of focusing strength
Engineering ：minimization and uniformity of the hardware, such as CM, SC cavities
Operation：the margin of operation VS design value
Optimization of “smoothness” from 2 to 10 degs !!
Baseline:

## Slide 14: End to end simulation
Emittance growth：
X/Y/Z: 4.5%/4.5%/4.4%
Acceleration efficiency >50%

## Slide 15: Rapid Recovery Stratrgy
Adaptive compensations scheme + AI
design
Cavity failure
Adaptive Compensation
DQN reinforcement algorithm flow chart
Beam envelope
Neural Network (Selector)
Neural Network (learner)
Memory Area
DQN error function
Envelope data
Lattice change quantity
Network data
Beam envelope data
Lattice change quantity
Beam function value
Network change
quantity
Memory data
Find the output energy threshold of each cavity type based on the velocity acceptance and matching requirements
Matching at low energy
Compensate energy at high energy
Iterative optimization to get the minimum cavity voltage redundancy
Type | 010 | 019 | 042 | 062 | 082
Redundancy | 20% | 15% | 10.7% | 6% | 10%

## Slide 16: High Power Target
Granular
liftor
A2T coupling
Heat ex.
Target loop
Diagnostic and
protection
tank
target
Emergency
collection
Granular
flow monitor
Neutron
monitor
Beam
diagnostics
volv
Spallation
neutron
Merits:
Heat exchange outside
No Stress due to beam trip
No thermal shock due to beam pulse
Drawbacks：
Dusty due to abrasion
Volume of target materials
Notes: 改模式，框图保留，加入CiADS系统之间的关系
加入流程图

## Slide 17: Design of Granular Target

## Slide 18: Subcritical Fast Reactor
 | Top level spec.
type | LBE sub- FR
Power | 10MWt (incl. beam)
fuel | UO2 (19.75%)
Keff | ~0.75
Main coolant Configuration | Pool-loop
Main coolant driven mode | Forced circulation
Coolant | LBE
Main coolant pressure | Normal
Main coolant temp | 280-380℃
main coolant exchanger | Main exchanger×2 Auxiliary exchanger×4
Main pump | Mechanical pump×2
Secondary Loop coolant | Pressure water
Secondary Loop pressure | 1.4MPa
Secondary Loop Temp | 225-260℃
Notes: 改模式，框图保留，加入CiADS系统之间的关系
加入流程图

## Slide 19: Nuclear design of reactor
19.75% UO2, 30 boxes
Neutron spectrum at the hot point
Neutron spectrum
(full energy range)
3.40E+14 n/cm2/s（at core）
Parameters | Unit | Value | 
 |  | BOL | EOL
Reactor Power | MW | 7.74 | 7.66
Target Power | MW | 2.26 | 2.34
Proton Energy | MeV | 500 | 
Beam Intensity | mA | 4.51 | 4.67
Neutron Yeild | n/p | 8.81 | 
Uranium Load | t | 1.7217 | 
EOL Burnup | MWd/tU | 4902 | 
Keff | - | 0.73457 | 0.72687
Ks | - | 0.76922 | 0.76450
Notes: 堆芯的核设计经过优化后，采用30组19.75%的燃料组件，提供7.74MW的堆芯热功率，采用低线功率密度燃料设计，平均线功率密度为34w/cm，堆芯最高线功率密度为42w/cm，极大的提高了运行的可靠性

## Slide 20: Coolant System Design

## Slide 21: Outlines
Background of Accelerator Driven System
Design Status of CiADS
Progress of Prototypes
  Accelerator, Target and Reactor
  Material SIMP
  New Approach of Fuel Recycle
Sammary

## Slide 22: Chinese ADS Front-end Demo linac (CAFe)
HEBT
DUMP
Beta=0.1
IMP
IHEP
Beta=0.21
Beta=0.15
IMP
162.5 MHz Taper HWR
IMP collaboration with IHEP 2011 ~ 2017
Supported by “Strategic Priority Research Program” of the Chinese Academy of Sciences.
ADS RFQ：2014-2017
(cooperation with LBL)
CMIF RFQ：2018-
Goal: to demonstrate 10 mA CW beam of superconducting front-end Linac for CiADS.
ions | P，H2+，α
frequency | 162.5 MHz
current | 10 mA
E in RFQ | 40 keV
E out RFQ | 3.1 MeV
Energy | 25/30/40MeV
Temp. | 4.5 K

## Slide 23: Commissioning of Superconducting Linac
162.5 MHz HWR010
4
5
2014.06.06——2014.07.24, RFQ
2014.09.14——2015.02.13, TCM1
2015.03.26——2015.06.29, TCM6, beam accident, RFQ AMP and coupler broken 2015.10.28——2016.01.21, TCM6 commissioning
2016.05.01——2016.06.20, injector II, coupler broken 2016.09.01——2016.12.17, injector II high power
2017.04.28——2017.06.18, CAFe, current leads broken 2017.10.03——2018.01.23, CAFe, operation stability 2019.01.04 ——2 mA CW beam, operation stability
Commission stage | First CW beam | Max Energy (MeV) | Beam time (hours) | CW beam time Total (hours) | CW Current Max(A) | CW Power Max(kW)
RFQ1/2 | Jun. 21, 2014 | 2.15/3 | 2036/~200 | 90/~120 | 11 | 23
TCM1 | Nov. 24, 2014 | 2.55 | 208 | 22.5 | 11 | 28
TCM6 | Jun. 24, 2015 | 5.3 | 400 | 20 | 4 | 21
Inject II | Sep. 24, 2016 | 10.2 | 327 | 11 | 2.7 | 26
CAfE | Jun. 7, 2017 | 26.1 | ~500 | ~140 | 2.55 | 45
3
162.5 MHz HWR010
2
162.5 MHz HWR010
1
162.5 MHz RFQ
Commissioning Goal: Higher power, Higher stability

## Slide 24: Operation Reliability Test with high power in 2019
Fist stage（15.8MeV@2.0mA）
Second stage（16.4MeV@2.1mA）
Stop to Change
current
and energy

## Slide 25: RAMI of CW beam with active MPS
No trip gap, 13.5 hours
Operation time 7553 min, downtime 737 min, availability 89%
Max power is 45 kW with 2.55 mA @17.5 MeV
Availability | MTBF | MTTR
0.89 | 90.7 min | 11.1 min
Availability | MTBF | MTTR
0.89 | 113.7 min | 14.6 min
1st stage: 2018/12/31 18:44 - 2019/01/02 23:42
2nd stage: 2019/01/04 08:08 - 01/07 09:03

## Slide 26: Operation for Users
Operation for users, Dec. 7th – 30th , 2018, May 14th ~June 30th 2019
Beam: H+ and 4He2+, energy 2.1-32MeV, average current 100nA~125uA
Available beam time 58.0 hours for 62 experiments
Downtime: 5.9 hours
Availability: ~ 0.90
source | trips
RF (incl. RFQ, LLRF) | 9
IS | 1
human | 4
control | 3
PS | 1
Diagnostic | 1
coupler | 2
total | 9

## Slide 27: Prototype of granular target
Electro-magnetic lifter
Heat exchange exp.
Integral target setup, verify granular flow, heat exchanger, electro-magnetic lifter, purifier, and so on
Granular flow
Granular temp.
Water temp.
Flux with aperture

## Slide 28: Zero-Power Lead Reactor
Experiments verified The accuracy of target-reactor coupling calculation and core design
operation monitoring system
Neutron count
time
II critical
I supercritical
III
IV
Target material | Period method/mk | Simulation /mk | Relative error/mk
Tungsten particles | -0.932 | -0.99 | -0.058
Tungsten | -1.144 | -1.162 | -0.018
Lead | 1.322 | 1.562 | 0.24

## Slide 29: LBE Loop & Oxygen Control System
Oxygen control setups
LBE Loop

## Slide 30: Outlines
Background of Accelerator Driven System
Design Status of CiADS
Progress of Prototypes
  Accelerator, Target and Reactor
  Material SIMP
  New Approach of Fuel Recycle
Sammary

## Slide 31: Smelting and Casting of SIMP
5 ton
Industrial grade !
1ton
5 tons
2 tons
2011
2012
2013
2014
2015
2016
5ton SIMP ingot
Control: purity, homogeneity
Upper-part texture
lower-part texture
Tensile properties
impact toughness
stable mechanical properties

## Slide 32: Evaluation experiments to SIMP

## Slide 33: General Evaluation
Tests | Result
TS/YS/elongation rate at RT-600℃ | SIMP > ( EP823, T91, RAFM )
Oxidation resistance at RT-800℃ | SIMP > ( EP823, T91)
LBE corrosion resistance (600℃, static saturation oxygen） | SIMP > EP823 > T91
LBE corrosion resistance (450℃, static saturation oxygen） | SIMP > T91
Short durability at 600℃ (150 MPa) | SIMP > ( EP823, T91)
Durability at 650℃ (100 MPa) | SIMP > T91 > EP823
Ion irradiation resistance at RT- 450℃ | SIMP > (T91, RAFM )
Ion irradiation resistance at 550℃ | SIMP > T91 > RAFM
SC water corrosion resistance (600℃, 25Mpa, 1000h) | SIMP > TP347, 304 SIMP > T/P91, T/P91
SIMP steels irradiated at SINQ-PSI, (n/p,  20dpa, 2012-2014)
Post Irradiation Examination (PIE) is under way, more results is coming.

## Slide 34: LBE Bump Prototype using SIMP
Panel / plate
Tubes/pipes
Φ60mm×10mm
Φ60mm×5mm
Φ60mm×1mm
Φ5mm×1mm
15mm
Liquid LBE centrifugal pump
30kW
2950r/min
The pump is currently being manufactured

## Slide 35: Outlines
Background of Accelerator Driven System
Design Status of CiADS
Progress of Prototypes
  Accelerator, Target and Reactor
  Material SIMP
  New Approach of Fuel Recycle
Sammary

## Slide 36: Technical Route of Reprocessing & Fabrication
Pulverization of UO2 pellets
Removal of the FPs from spent nuclear fuels
Preparation of ceramic nuclear fuel microspheres
Technical route
Notes: The picture is Technical route of the Production and Reprocessing of Nuclear Fuels.

## Slide 37: Pulverization of Pellets & Removal of Volatile FPs
Removal of the volatile fission products from spent fuel by the Voloxidation Process
Element | Mo | Cs | Ru | Te | Rh | Se
Removal% (1200 ℃) | 95 | 90 | ~50 | 82 | ＜5 | 100
Pulverization & Ox/Re of real UO2 pellets
Oxidation：air, 450 ℃, 4 h
Reduction：4% H2-Ar, 700 ℃, 4 h
Notes: Pulverization of UO2 pellets are accomplished by oxidation - reduction Process . This is a nonmechanical method for the pulverization of sintered uranium dioxide fuels suitable for use as an economical procedure for the low decontamination reprocessing of such nuclear fuels.
Removal of the volatile FPs by the Voloxidation Process. Iodine, and the volatile fission gases are released from the spent fuel at high temperatures. The separations processes rely on the ability of some actinides and fission products to form volatile or semi-volatile oxides.

## Slide 38: New Approach to Spent Nuclear Fuel Recycle
Highly Efficient and Selective Dissolution Separation of Fission Products from Spent Nuclear Fuels by an Ionic Liquid, [Hbet][Tf2N]
Fang-Li Fan et al., Inorg. Chem. 2019 58(1) 603-609
Notes: This innovative method allows the selective dissolution of neutron poisons, lanthanides oxide, as well as some fission products with high yield, leaving most of the UO2 matrix and minor actinides behind in the spent nuclear fuel and accomplishing the actinides recovery as a group. This approach features a little waste and efficient selectivity, mild conditions, which opens up a new avenue for simple, convenient, sustainable, and green for the spent nuclear fuel reprocessing.

## Slide 39: Preparation of ceramic nuclear fuel microspheres
In-situ mixing internal gelation-microwave heating device
Preparation of UC ceramic microspheres by an improved microwave-assisted rapid internal gelation process combined with carbothermic reduction
Optical image of
UC ceramic microspheres
UC ceramic microspheres
size: Ø 675 µm
density : 12.53 g/cm3 (92% TD)
Wei Tian et al., Ceramics International 44 (2018) 17945–17952
Notes: Uranium monocarbide (UC) ceramic fuel has been considered as a potential nuclear fuel because of its high thermal conductivity, high melting point, good mechanical property and high uranium atom density.
In our work, uniform sized ceramic UC microspheres were prepared by an improved microwave-assisted internal gelation combining with carbothermic reduction process. The UC ceramic microspheres have an average diameter of 675µm and a density of 12.53 g/cm3, which is 92% of the theoretical density. So, this method can provide an important guidance for the preparation of Pu and MAs carbides microspheres for nuclear reactors in the future.

## Slide 40: Outlines
Background of Accelerator Driven System
Design Status of CiADS
Progress of Prototypes
  Accelerator, Target and Reactor
  Material SIMP
  New Approach of Fuel Recycle
Sammary

## Slide 41: Sammary
The ADANES was proposed as a new closed fuel cycle system, aiming sustainable nuclear energy.
The CiADS (prototype of ADB) started earthwork in last August. It is planned to be the first commission in 2024.
The front-end demo CAFe (25 MeV superconducting linac) started commissioning in 2017. It has achieved max beam power of 45 kW with 2.55 mA @ 17.5 MeV. It operated at 2 mA more than 100 hours. 100 kW beam power, rapid recovery and long-term operation is the next goal.
The granular flow spallation target was proposed to be a candidate for 10 MWs application. A prototype was built and tested.
The SIMP steel was developed for the use to LBE related nuclear energy systems. The experimental results show that its property could be better than other candidates.
The new recycle procedures of Spent Nuclear Fuel for ADB was proposed, and it is proved with SIMFUEL in IMP laboratory.

## Slide 42: Thank you! Welcome collaboration!
Thanks our team and worldwide collaboration in the past!