## Slide 1: Development of Elliptical Cavities in IMPCAS
Yulu Huang
On behalf of the CiADS SRF group

## Slide 2: OUTLINE
Background Introduction and Basic Parameters
1
Main concerns in Our Elliptical Cavity Design
2
Worldwide Performances and Limitations
3
RF Design
4
Mechanical Design
5
Prototype, Post-processing and Test System Status
6
Summary
7

## Slide 3: Background-CiADS 500 MeV Demo Facility
Particle | proton | 
Energy | 500 | MeV
Beam current | 5 | mA
Upgradeability | 10 | mA
Operation mode | CW& Pulse | 
Beam loss | ＜1 | W/m
175 MeV

## Slide 4: Specification From Related Systems
Accelerator Physics
LLRF
Cryogenic
SRF
vacuum
alignment
vibration
solenoid
…
Beam Dynamics
Power Supply
…
2018-9 international review
2019-4 internal review
2019-9 international review
 | Cavity | unit | Ellip.062 | Ellip.082
Accelerator Physics | βopt |  | 0.62 | 0.82
 | Frequency | MHz | 650 | 650
 | Aperture | mm | 100 | 100
 | Cell Number |  | 6 | 5
Cryogenic | Temperature | K | 2 | 2
 | Helium Pressure Fluctuation | Pa | ±10 | ±10
 | Max stress in helium vessel（RT） | bar | 2 | 2
 | Max stress in helium vessel（2K） | bar | 4 | 4
LLRF | Bandwidth | Hz | 220 | 220
 | LFD coefficient | Hz/(MV/m)2 | <1 | <1

## Slide 5: Main concerns in Our Design
Helium pressure, 2bar(RT), 4bar(2K)
Cool down to 2K
Tuning
High Eacc, High Q0
Low Qext（2.95E6）
High Order Modes
Lorentz Force Detuning
Epk and Bpk limitation（operation Epk）
Rres（Q0 and Cryogenic losses）
Balance between Vacc and Plosses
Stress Analysis
Main coupler design，
Coupler kick，
Increase the beam pipe…
Cryogenic losses;
Emittance growth，energy spread, BBU …
HOM coupler or not?
Helium vessel and stiffening ribs design
Tuner Design
LFD coefficient less than 1 Hz/(MV/m)2

## Slide 6: Epk Limitation
Epk/Eacc=2.19
Epk in operation with 60pps bunch:
  LB804 :24-43 MV/m
  HB804:20-36 MV/m
SNS 805MHz Cavities
ESS 704 MHz Cavities_VT
PIP II 650 MHz Cavities_VT
Epk/Eacc=2.71
Epk/Eacc=2.36
CiADS Elliptical Cavities Operation Epk=29 MV/m
Consider:
Performance degradation from VT to operation
Cryogenic and RF power supply budget
Long time stable operation
Epk >40 MV/m
Epk >40 MV/m

## Slide 7: Bpk Limitation
325 MHz: Bpk < 60mT
650 MHz: Bpk < 70mT
1300 MHz: Bpk < 80mT

## Slide 8: Residual Resistance
 | SNS(MB) | SNS(HB) | ProjectX
βG | 0.6 | 0.8 | 0.9
Frequency, MHz | 805 | 805 | 650
Bmax/Eacc | 5.72 | 4.72 | 3.75
Bmax, mT | 72 | 72 | 72
Eacc, MeV/m | 12.6 | 15.2 | 19.2
G, Ω | 179 | 260 | 255
Q0 meas.(at Bmax=72mT) | 2∙1010 | 1.8∙1010 | 3∙1010
Measur: Rs=G/Q0 , nΩ | 9 | 14 | 5
Rres = 5-10 nΩ
RBCS = 4.2 nΩ
SNS Cavities(805MHz)
CiADS Cavities(650MHz)
Rtrap = 4.84 nΩ
RBCS = 2.73 nΩ
Rres = 10 nΩ
Rsurf = 17.57 nΩ

## Slide 9: Operation Target
20W (more or less) Cryogenic losses@:
Epk=29 MV/m (Operation)
Rsurf=10+2.73+4.84(20mG)=17.57nΩ
Relatively Conservative!

## Slide 10: RF Design-Geometry
Fixing riris=50mm for both 062 and 082 cavities due to beam dynamics requirements.
Fixing wall angle alpha=2 degree for both the middle cell and the end cell
The midcell half cell length are determined by their optimum betas
For tuning in each optimization step
3 independent parameters!

## Slide 11
Coutour Plot of G*R/Q VS Epk/Eacc and Bpk/Eacc
Parameter Sweeping Results
062_G*R/Q
082_G*R/Q
082_G*R/Q

## Slide 12
Cryogenic Losses Estimated @Epk=29MV/m,Rs=17.57nΩ
062
082
Parameter Sweeping Results

## Slide 13: Final Geometry
Cavity | 6 Cell 062 |  | 5 Cell 082 | 
Cell | Middle | End | Middle | End
Equator Dia. 2D (mm) | 395.346 | 395.346 | 393.003 | 393.003
Iris Dia. 2r (mm) | 100 | 110 | 100 | 110
Half-cell length L (mm) | 68 | 72 | 89.6 | 89.2
Iris b (mm) | 22 | 22 | 30 | 30
Iris a (mm) | 13.61 | 17.79 | 17.86 | 17.63
Equator B (mm) | 59 | 59 | 70 | 70
Equator A (mm) | 52 | 52 | 70 | 70
Wall Angle (degree) | 2 | 2 | 2 | 2
End-Cell Sl (mm) | 0 | 0 | 0 | 0
Beam pipe length Ltube (mm) |  | 198 |  | 162
Beam pipe diameter Dtube (mm) |  | 110 |  | 110

## Slide 14: EM Parameter
Parameter | LB650 | HB650
Cell number | 6 | 5
βopt | 0.62 | 0.82
TTF_opt | 0.72 | 0.74
Epk/Eacc | 2.80 | 2.10
Bpk/Eacc（mT/(MV/m)） | 4.86 | 3.98
R/Q(Ω)_βopt | 334 | 501
G | 187 | 229
Field Flatness | 98.76% | 99.48%
Coupling Factor k | 1.54% | 0.96%
Leff | 0.824 | 0.895
Ltotal | 1.22 | 1.22
Epk_Operation | 29 | 29
Eacc | 10.36 | 13.81
Vacc | 8.54 | 12.36
Bpk | 50.37 | 54.96
Rbcs（2K） | 2.73 | 2.73
R0 | 10 | 10
Rtrap（20mG） | 4.84 | 4.84
Q0 | 1.1e10 | 1.3e10
Ploss(2K) | 20.52 | 23.41

## Slide 15: Normalized Electric Field and TTF
(0.62,0.723)
(0.82,0.74)
175-377MeV
0.542-0.7
>0.55
377-1000MeV
0.7-0.875
>0.56

## Slide 16: RF Power Coupling
Bandwidth 220Hz for both LB650 and HB650
Different values of L and D are shown for QL=2.95E6
D
L

## Slide 17: High Order Modes (HOMs)
TM Modes
TE Modes(No couple to the beam)
Monopole_TM0np
Dipole_TM1np
Quadpole_TM1np
And higher…
Dipole_TE
Quadpole_TE
And higher…

## Slide 18: HOM Issues
Emittance degradation
Energy spread
Beam-Break-Up (BBU)
Cryogenic loading (Incoherent and Resonating)
=

## Slide 19: HOM Power Spectrum
Phom-total=0.57mW
Phom-res-5M=172mW
162.5MHz CW single time structure；
Gaussian bunch，rms length is 1mm；
Beam current 10 mA；
Time Averaged HOM Power Spectrum Normalized to R/Q_062

## Slide 20: Monopole Impedance Spectrum

## Slide 21: Dipole Impedance Spectrum

## Slide 22: MP Analysis
MultiPac 2.1
CST-Particle Tracking
CST-PIC
300 degree bakeout Nb
Initial electron energy 4eV with 200% spread，initial angle +/-45 degree
End cell and middle cell，Eacc=1-20MV/m sweeping, no MP

## Slide 23: Mechanical Design
Scissor tuner
bellows（RT tuner）
SS flange and helium vessel（sealing，cost，fabrication）
4 mm Nb sheet, post-processing to 3.8 mm
Double stiffen rings（LFD）
Similar mechanical design for both 062 and 082 cavities.

## Slide 24: Lorentz Force Detuning Analysis
Boundary Conditions：
Uz=0
Tuner is simplified to a spring with unknown stiffness
Calculating the LFD coefficient with different tuner stiffness
When tuner stiffness is larger than 30kN/mm，LFD coefficient less than 1 Hz/(MV/m)2

## Slide 25: Df/dp analysis
Boundary Conditions：
Uz=0
Tuner is simplified to a spring with unknown stiffness
Calculating the df/dp with different tuner stiffness
Helium pressure fluctuation is within +/-10 Pa in 2K system
Df/dp requirement for PIP II is less than 25Hz/mbar, tuner stiffness need to be larger than 25kN/mm.

## Slide 26: Tuning Sensitivity Analysis
Tuning sensitivity =209kHz/mm
Cavity longitudinal stiffness=2.6kN/mm

## Slide 27: Stress Analysis
P3-Beam Vacuum
P1-Pressure in Lhe volume
P2-Insulating Vacuum
Boundary conditions：
Uz=0
Consider：Gravity，cool down，tuning，pressure…
Make sure equivalent stress on the cavity and helium vessel less than their yield strength
RRR300 Nb Yield strength：RT 50MPa，2K 450MPa
316L SS Yield strength ：RT 250MPa，2K 550MPa

## Slide 28
Load case 1：
（1）Gravity
（2）P1=0.205MPa
（3）P2=P3=0
Load case 2：
（1）Gravity
（2）P1=0.4MPa
（3）P2=P3=0
（4）Liquid Helium
Load case 3：
（1）Cool down to 2K
（2）Tuner Extension of 2 mm
RT，Nb<50MPa, SS<223MPa
2K，Nb<52MPa, SS<52MPa
2K，Nb<98MPa, SS<445MPa
Stress Analysis

## Slide 29: Stress Analysis
Load case 4：
（1）Gravity
（2）P1=0.4MPa
（3）P2=P3=0
（4）Liquid Helium
（5）Cool down to 2K
（6）Tuner Extension of 2 mm
Load case 5：
（1）Gravity
（2）P1=0
（3）P2=P3=0.1MPa
2K，Nb<148MPa, SS<447MPa
RT，Nb<45MPa, SS<138MPa

## Slide 30: 650 MHz Single Cell Prototype Cavities
3 single cell 650 MHz elliptical prototype cavities
Made from 3.5 mm niobium sheet (less than our designed 4 mm)
Expected be ready for VT test at the end of this year

## Slide 31: 650 MHz Elliptical Cavity EP System
Based on the 1.3GHz elliptical cavity EP system
Electrode optimization to fit the small wall angle (2 degree)
Expected to be available at the end of this year (2019)

## Slide 32: Multi-cell Cavity Pre-Tuning System

## Slide 33: Summary
RF Design and Mechanical Design of the CiADS 650 MHz elliptical cavities (062 and 082) were finished.
3 single cell prototype cavities were fabricated and will be test at the end of this year
Multi-cell prototypes with helium vessels are on the way…

## Slide 34
Thanks for your attention!