## Slide 1: Status of the HZG-Demo detector project:
Development of mechanics, coatings, electronics and software in one group and an external partner (S-DH GmbH)
G. Nowak, J. Plewka, Ch. Jacobsen, C. Gregersen,
F. Theopold, A. Beldowski, W. Puls, J. Burmester,….
Budget: 672 200,00 Euro
Period 24 months (started 30.07.2018)
Aim of current project: Demonstrator detector specs:
1m2 active area
3 detection planes
2 mm x 5 mm position resolution
Linear response up to a count rate of 800 kHz
Efficiency for 2 Å neutrons ≈ 20%
/n sensitivity: 10-6
Infrastructure and Team at HZG :
-Building with clean room, Vernier press, (neutron Lab-source),..
Demonstrator detector project definition:

## Slide 2: Long-term aimed detector performance:
„Wish-list“ for neutron diffraction detectors:
sample-detector distance: 2 m:
active area: 1 m x 1m
efficiency: η > 60 % (@ 2 Å)
position resolution: 2 mm x (5 mm)
max. countrate:< 106 1/s (global)
mobile design (max. 800 kg)
price < 3He-technology
…

## Slide 3: Neutron Detection Process
-A. Rose, “Sputtered Boron Films on Silicon Surface Barrier Detectors” NIM methods,52,166-170, (1967)
Al-substrate
10B4C-converter
CF4 - stopping gas
cathode (y)+DL
anode (x)+DL (HV)
r7Li
rα
TDC
y
x
1 µm
x
y
2D-intensity
Neutron was there!
α
--
+
n + 10B → 7Li + α + (γ)
10B4C-converter
Al-substrate
n
-G. Nowak, M. Störmer, H.-W. Becker, C. Horstmann, R. Kampmann, D. Höche, M. Haese-Seiller, J. - F. Moulin, M. Pomm, C. Randau, U. Lorenz, R. Hall-Wilton, M. Müller,
A. Schreyer, J. Appl. Phys., 117, 034901 (2015)
-European Patent Application WO2016/008713

## Slide 4: Detection strategy
Stacking of detection planes
Delay-line read-out
High timing control
Detector geometry independant on
sample-detector distance
*F. Piscitelli and P. Van Esch JINST 8, P04020, 2013
Efficiency simulations by
Dr. I. Stefanescu (ESS-DG):

## Slide 5: Status of neutron detector project: design and construction @ TKE and TKA
Design detector coating: arrived! assambly: in work
1000 mm
Detector design: ready!
1000 mm
≈1460
-weight: currently 600 kg
Detector electronics
integration: ready!
1200 mm
1165 mm
1165 mm
Large area sputtering system at
S-DH GmbH:
First 2x “1m2”coatings:
-all 8 1m2 coatings (1.2 µm thick 10B4C on Al) arrived at HZG
on time and are ready for installation in neutron detector.

## Slide 6: 1m long wire under mechanical in HV-E-field
1200 mm
Set-up for wire tests:
wire position
over ground
-15-20 µm wire has an optimum mechanical performance
for the aimed application
Tension limits for wire:
10 µm: 0.34-0.38 N
15 µm: 0.66-0.68 N
20 µm: 0.90 N
30 µm: 2.1 N
Results of wire tests:

## Slide 7: 1m long wire under mechanical in HV-E-field (b)
Set in of transversal wire oscillations (≈100 Hz):
Sparking during transversal wire oscillations:
-to low mechanical tension!

## Slide 8: Converter deflection-Force Compensation Volume
Minimize bending with force compensating volumes
X-delay lines
Y-delay lines
10B4C coatings
~1200mm
~200mm
neutrons
force compensating volumes
detector elements
individual pressure control
filed European Patent: EP 17184906.0 (04.08.2017)

## Slide 9: Converter deflection control
Set-up for first converter deflection control tests
back side (simulation of deflection) :
front side:
Demo:
Reflection of
a laser beam
10 mm

## Slide 10: Preliminary Pulse height spectra tests ( vs. ) discrimination
HV/preamp/main amp.
241Am (40kBq)
Scope/MCA
Ar/CF4 (80%/20%) @ 1.1bar (0.1bar overpressure)
HV to ground: 0 - 4000 V
Set-up:
without_paper
10µm W/Au-wire
20mV/div


Histograms of significant variables for AI-analysis:

## Slide 11: Development, assembly and integration of electronics
Preamp (30 dB):
Motherboard with 8 (CFD)
-fully differential
-ADC (scope mode)
CFD-board:
Zynq board:
HV-delay-line:
First pulses:
Main-amp., CFD, FPGA(TDC)-unit for 2 planes:
Detector electronics integration:
-“connection“ to ICS/EPICS integrated
Software:
Currently: web-interface in development

## Slide 12: Electronic and software tests @ V20-ESS-test beamline:
1000 mm
Developed Electronics & Software:
Set-up for basic “imaging” with a
conventional 3He detector
First „neutron images“ reconstructed by newly developed Electronics & Software:

## Slide 13: Timing synchronization
TDC written in FPGA:
(Δt = delay-time  neutron @ (x(Δt),y(Δt),respective plane, ToF))!
-FPGA with internal timing base (≈ 200 ps)
-1.1 ns delay time step for one wire
ESS-D.net
ICS
n @ (x(Δt),y(Δt),n-p,ToF)
Time mark every 0.1 s
for n-p, ToF

## Slide 14: Conclusion and Summary
-detailed detectordesign ready
-coatings in place
-read-out electronics in final stage and teste
-Infrastructure at HZG grows up; infrastructure
for n-source is delayed.
To do:
-wiring and soldering of detector wire
-assembly
-Irradiation of converter under high flux
Thanks to our team!:
Jörg Burmester, Jörn Plewka, Christian Jacobsen, Carsten Peter Gregersen, Wolfgang Puls, Andreas Beldowski, Dirk Jan Siemers, Rüdiger Kiehn, Sven Kleeband, Thorsten Böttcher, Gerd Musielak, Erik Sitko, John Hedde
Thanks to the colleagues from the
ESS-detector group!
Thank you for your attention!

## Slide 15
Back-up’s:

## Slide 16: Detector Lab
clean room
veneer press
Safe
Neutron source
Detector
shelves
shelves
shelves