## Slide 1: SPL cavity construction: Status and lessons
On behalf of SPL team

## Slide 2
Overview
Niobium cavities
R&D
Conclusions
Material procurement
Monocell
5–cell cavities (Research Instruments) x 4
5–cell cavity (CERN)
Helium tanks

## Slide 3: Overview
Cavity
Helium tank
Inter-cavity
support
Thermal shield
Vacuum vessel
RF coupler
Thermal shield tie-rod
Cold-to-warm
transition
Magnetic shielding
Insulation vacuum
relief plate
Cryogenic circuit
burst disk
Gate valve
Two-phase pipe
Cavity tuner
Double-walled
tube
He phase separator
Cryogenic lines port
Thanks to R. Bonomi and V. Parma

## Slide 4: Overview
Bulk Niobium 5Cells cavity
Stainless steel (316L /316LN) helium tank designed by CERN, supplied by CEA and welded to the cavity at CERN.
4 niobium cavities delivered by Research Instruments
Tuners provided by CEA. Under testing at CERN
Pumping line & Magnetic shield to be provided IPN Orsay.

## Slide 5: Overview: 5-cell Cavity
PROPERTIES
5-cell cavity β=1
Material: Bulk Niobium RRR300
Flanges: 316LN
Frequency: 704.4 MHz
Quality factor: 1010
Nominal gradient Eacc= 25 MV/m
Cavities:
4 niobium 5-cell cavities β=1 by Research Instruments (RI)
1 niobium monocell by RI
1 niobium 5-cell cavity β=1 under fabrication at CERN
2 copper 5-cell cavities β=1 (prototypes) fabricated at CERN

## Slide 6: Niobium cavity-Material procurement
Plates
Seamless tubes
Company | Price | Lead time | Qty
A | 472 € / Kg | 16 months | 72 plates
B | 503 € / Kg | 10 weeks | 8 plates
High prices
Bad tolerances
Problems during fabrication: overlapping
To avoid welds which could lower the RRR value.

## Slide 7: Niobium cavity-Material procurement
Grain size is not that important (at least for fabrication), and it was accepted material with bigger GS than initially wanted (up to G = 4)
Seamless tubes are extremelly difficult to fabricate with the good tolerances, and we believe that surface defects appear during their fabrication. It is recomended for the fabrication of the end groups to opt for the bent + weld solution or spinnig from plates
Lessons learnt:
Notes: Machining in the inside of the spun tubes is required as the surface finishing is not as specified

## Slide 8: Niobium cavity-Monocell from RI
Threefold purpose:
Validate RI fabrication processes (forming, welding, brazing)
Electropolishing tests
Cold tests

## Slide 9: Niobium cavity-Monocell from RI
Material defects made evident after EP

## Slide 10: Niobium cavity-Monocell from RI
Cutting of the monocell in order to inspect the defects and assess their origin
Different defects were inspected in several cross sections
Shallow
No progression
Aspect of chemical dissolution
Surface discontinuities most likely are originated during fabrication and / or handling emphasised after EP

## Slide 11: Reparation monocell from RI at CERN
The monocell was repaired in order to continue with the electropolishing and cold tests.
EB Welding from the outside (W#3)
Full penetration: 1.7 mm
Cross section of the EB weld (W#1 +W#2)
Cross section of the EB weld (W#3)
EB Welding from the outside (W#1) and inside (W#2)
Full penetration: 2.4 mm
Notes: The monocell was repaired in order to continue with the electropolishing and cold tests.

## Slide 12: Niobium cavities at RI
4 niobium cavities fabricated by Research Instruments (RI) arrived to CERN Dec. 2013.

## Slide 13
Differences in fabrication RI versus CERN
EB welding with step joint design
EB welding with butt joint design
EB welding of the complete cavity in vertical- no need of special tooling
EB welding of the complete cavity in horizontal position- special tooling neede
RI
CERN
Electron beam
Electron beam

## Slide 14: Niobium cavities-RI
Studies at CERN to optimize the necking out parameters in order to minimize the deformation:
  Ellipse diameters
  Necking height
  Tooling
The new set of parameters (which gave satisfactory results at CERN) were adopted by RI for the necking out of their end groups
For the end groups to be done at CERN, a specially dedicated tooling has been designed and is under construction
Challenge: Necking – out of the end groups
All material properties were according to the specification but the material cracked due to excessive deformation.
Lesson learnt:

## Slide 15: Niobium cavities-RI:Dimensional contol
 | CAVITY 1 | CAVITY 2 | CAVITY 3 | CAVITY 4
Run-out 0.5 /A-B | 5.359 | 7.725 | 5.223 | 4.714
Length of the cavity 1397.3 ± 3 | 1395.886 | 1393.831 | 1395.592 | 1395.229

## Slide 16: Niobium cavities-RI
If we measure the center point of the cells and the extremity flanges we can see that there is huge deviation. The cells are shifted with respect to the axis defined by the extremity flanges.
 | Cavity 1 | Cavity 2 | Cavity 3 | Cavity 4
Axis straightness (of the 5-cells) | 1.075 | 1.803 | 1.167 | 1.078
Concentricity (between axis AB and the axis created by the 5-cells) | 5.014 | 6.883 | 4.282 | 4.240
Cylindricity (of the 5-cells) | 1.308 | 2.122 | 1.372 | 1.330
Cavity 2
Thanks to S. Mikulas and A. Macpherson
Field flatness value 3.26 %

## Slide 17: Niobium cavity at CERN
Spinning of half-cells and beam tubes at HEGGLI
Extensive testing has been done in order to optimize the spining parameters and tooling to achieve the required tolerances. It was proven that it is a process difficult to control and the results were not as expected . New forming techniques are being considered

## Slide 18: Niobium cavity at CERN
Dimensional control by CMM
RF measurements
Machining of the iris (at CERN)

## Slide 19: Niobium cavity at CERN
Spinning
Machining
Cutting cell length
RF measurement
CP (chemical polishing)
Spinning
Machining – Welding preparation (Iris & rings)
CP
Nb
HALF-CELLS
RF measurements
Assembly half-cell+ half-cell+ stiffening ring=> Dumb-bell
Degreasing + CP (8 h before EBW)
EBW half-cell + half-cell
Degreasing +CP (8 hours before EBW)
EBW dumb-bell+ stiffening ring
RF measurements
Trimming equators
RF measurements
Grinding and CP (if needed)
DUMB-BELLS
EBW
EBW
CP
EBW
Trimming equators
Grinding and CP (if needed)
EBW
Degreasing +CP
Nb
Spinning
Necking-out
Machining
CP
Spinning
Necking-out
Machining
CP
BEAM TUBES

## Slide 20: Niobium cavity at CERN
Nb
Machining SS Flange + Nb beam tube + SS insert
Degreasing + CP
Brazing
Machining-Removal of SS insert
Machining
Brazing
SS
TANK CONNECTOR
EBW
2
Assembly beam tube + ports=> end group
Degreasing + CP ( 8h before EBW)
Electron beam welding (EBW)
CP
END GROUP
Machining SS Flange + Nb tube + SS insert
Degreasing + CP
Brazing
Machining- Removal of SS insert
Brazing
Machining
Nb
SS
FLANGES
SS
Degreasing
BEAM FLANGES
Machining SS Flange + Nb beam tube + SS insert
Degreasing + CP
Brazing
Machining-Removal of SS insert
Brazing
Machining
SS
Degreasing
SS
Nb
SS

## Slide 21: Niobium cavity at CERN
RF measurements
Trimming
EBW
EBW
RF measurements
EXTREMITY 1
EBW
CP
Cp
Assembly end group+ tank connector + half-cell=> extremity 1
Degreasing + CP ( 8h before EBW)
EBW end group + tank connector
Degreasing + CP ( 8h before EBW)
EBW end group + half-cell
RF measurements
Trimming equator
RF measurements
Assembly end group + half-cell=> extremity 2
Degreasing + CP ( 8h before EBW)
EBW end group + half-cell
RF measurements
Trimming equator
RF measurements
EBW
Trimming
RF measurements
RF measurements
EXTREMITY 2
CP

## Slide 22: Niobium cavity at CERN
Final assembly
CP - 8 h before each EBW
EB Tack weld
EBW
EB Tack weld
EB Tack weld
EB Tack weld
EBW
EBW
EBW

## Slide 23: Niobium cavity at CERN
New EB welding machine at CERN (11 m3);
SS vacuum chamber;
Vacumm level 10-5 mbar up to 10-7 mbar (cryo. pump) Suitable for high RRR niobium welds (see R&D  RRR).

## Slide 24: Tunning tests: Cell – by – cell tunning system
Cell-by-cell tuning system with RF bead-pull measurements
Mechanical measurements: frequency shift with respect to stress and deformation
Measured cavity frequency change vs. mechanical deformation of cell no 4.
The tests were done with a prototype copper cavity
Thanks to M. Guinchard

## Slide 25: Tunning tests: cavity tunner
Chart: Deformation in fonction of the frequency
| -1.9000000000000001E-4 | -0.49790000000000001 | -0.99750000000000005 | -1.5089999999999999 | -2.0270000000000001 | -2.5219999999999998 | -3.0049999999999999 | -3.22 | 0.1033 | 1.101 | 2.1120000000000001 | 3.0939999999999999 | 3.8780000000000001
 | 0 | -0.0428 | -0.1104 | -0.1731 | -0.2347 | -0.2954 | -0.3533 | -0.3785 | 0.0002 | 0.0413 | 0.1454 | 0.2321 | 0.3036
Cavity tuner: measurement of cavity detuning versus mechanical deformation.
The tests were done with a prototype copper cavity
Thanks to M. Guinchard

## Slide 26: Tunning tests: cavity tunner
Tunning tests are being repeated with a niobium cavity

## Slide 27: Procurement of He tanks
5 stainless steel (316L / 1.4404) helium tanks designed by CERN and ordered by CEA have been fabricated at SDMS.
Many dimensions are out of tolerances and we are checking if they are acceptable.

## Slide 28: Procurement of He tanks
When defining the technical specification, it was not considered any restriction regarding the filler metal for the longitudinal weld, what ended with a high magnetic permeability in this region.
In order to avoid this, a filler metal with very high Nieq should be specified
If permeability is a paramount concern, the tank should be made in 316LN
316L
Filler metal

## Slide 29: R&D- Brazing
Brazing Nb / SS 316 LN with a Cu-OFE copper interface is a key technology developed at CERN in 1987
Niobium cavity & SS tank
SS flanges
Difference in expansion of Nb/SS
Nb tube fitted to SS flange
Clearance ≤ 20 µm
SS plug to expand the Nb
Cu – OFE copper as brazing material
Brazing temperature 1100°C, ∆time <<
P< 10-5 mbar

## Slide 30: R&D- Brazing
The joint proved to be functional and to mechanically fulfil the requirements for the intended application
It was also decide to mask the brazed joint during EP operations to avoid damaging its soundness
It was proven that an EB welding close to the brazed joint does not affect the interface
Nb tube + SS flange
Full results in presentation
I. Aviles and N. Valverde SLHiPP2
SS
Nb

## Slide 31: R&D- Welding tests
Ti6Al4V
Ti6Al4V
Nb55Ti
Nb55Ti
Nb
Nb
Still trying to find the good parameters

## Slide 32: RRR measurements
Chart: Distance to weld bead (mm)
| 0 | 2.5 | 5 | 10 | 15 | 20 | 40
SST no getter | 417.319 | 418.8122 | 409.6083 | 416.7053 | 421.0137 | 413.6498 | 412.344
PTR no getter | 400.6168 | 408.7669 | 440.492 | 437.397 | 438.2755 | 438.6963 | 439.0878
@ lower vacuum levels  degradation of 10% of RRR value
@ higher vacuum levels with the new EB welding machine  RRR value does not degraded apart from statistical variation
SST  3.3  10-5 mbar
PTR  1.3  10-4 mbar

## Slide 33: Conclusions
Material procurement: Seamless tubes are to be avoided as the rolling + welding or spinning of the end groups is easier and well performing.
Niobium 5-cell cavities: 4 cavities were fabricated at RI. Dimensional tolerances are not fulfilling the specification, but RF measurements at RT were satisfactory. We are still performing tests (EP, HT, cold tests…)
Niobium 5-cell cavity at CERN: forming of the half cells has been done together with the brazing of the ports. EB welding tooling has been fabricated and soon we will start with the welding of the dumb – bells.
Helium tank: It has to be considered the magnetic susceptibility of the material and the filler metal if aplicable.
Brazing: It has been proven that it is a successful solution for the Nb/SS interfaces for superconducting cavities. Tests at cryogenic temperatures are foreseen.
Welding tests: First trials were not as expected but new welds will be carried out soon with improved welding parameters.

## Slide 34
Thanks for your attention!!
We would like to thank the people who help us in our work:
G. Arnau Izquierdo, S. Atieh, K. Artoos, O. Capatina, JM Dalin,
L. Ferreira, S. Forel, A. Gerardin, M. Guinchard, M. Malabaila,
F. Pillon, A. Porret, D. Pugnat, M. Redondas, T. Renaglia, T. Tardy, A. Vacca