## Slide 1: Paul Scherrer Institut
12. Mai 2014
PSI,
Design and performance of the copper collimator KHE2 in the 590 MeV beam line at PSI
Daniela Kiselev, Pedro Baumann, Daniel Laube,
Davide Reggiani, Raffaello Sobbia, Ake Strinning
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 2
Proton beam line from Target E to KHE2&3
Target E:
purpose: meson production
4 cm graphite wheel
rotating with 1 Hz
additional beam spread:
~6 mrad
590 MeV
Protonen
Target E
KHE0
KHE1
KHE2
KHE3
5m
beam losses: 13% 16%
Collimator system: OFHC-Cu
- protection of the beam line
reduction of beam losses
(activation)
large power deposition
@ 2.4 mA:
152 kW in KHE2
34 kW in KHE3
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 3
Active cooling:
steel tubes (coated with Cu)
brazed with SCP1 at 850 oC on Cu
5.3 m/s (limit for Cu-tubes would be 2-3 m/s)
4 Thermocouples (TC) for
temperature controlling
4 slits for thermal expansion
400
500
600
2mA
protons
K
Y.J. Lee
@ 2.4 mA: ~ 400 oC
engineering limit:
homologeous temperature
= ½ of melting temperature in K
= 405 oC
 limit reached!
Temperature distribution: max: 380 oC @ 2 mA
The collimator KHE2
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: Dimension: 26 cm Durchmesser, 16 cm vertikale Öffnung, 8 cm horizontal

## Slide 4
Diaphragm in front of KHE2
PIC
127 mm Ni- foil, isolated from KHE2:
production of secondary electrons
small current
measure of beam position
included in interlock system
online monitoring in control room
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 5
Shielding
2.5 m
Concrete shielding
Working platform
Target E
Collimators
5 m
inflatable
seals
4 m
Concrete shielding can be removed
by crane
Inserts can be removed
by exchange flask & crane
Steel shielding: ~ 2.5 m
Local shielding:
10 cm Cu, water cooled
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 6
Shielding
Local shielding around the
collimator
cooling plate
main shielding
can be removed
remotely
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 7
Remote control and measures for Radiological safety
dosimeter: up to 45 Sv/h measured
Radiological control:
dose measured at several locations
Tritium monitor
Contamination protection: box around,
air is sucked out
dose rate at surface of the exchange flask:
< 2 mSv/h
box against contamination
air sucking
bridge
door
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 8
remotely movable table
stand
service cell
Pb-window
1 m
parking slot1
shielded with 50 cm heavy concrete
and 20 cm steel
sluice
parking slot2
Transportation in parking slot or service cell
control room
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 9
Dose rate of KHE2
KHE2
downstream
upstream
measured
calculated
dose rate [Sv/h]
distance [cm]
p
Ni aperture (127 micron)
highest dose ever measured at PSI West, limit of the dose meter: 500 Sv/h
MCNPX
+ Cinder’90
after 19 years of operation and 3 months cooling (March 2009)
in general: components after TargetE have dose rate between 1-10 Sv/h
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 10
Reasons for the inspection of KHE2 2009 (after 19 years)
1) Operation reliability:
after 19 years of operation: end of life time?
no replacement at hand: would take ~3/4 year
For the new KHE2&3 design:
Is OFHC-Cu a good choice ? (alternative Glidcop)
radiation damage?
change of mechanical properties:
cracks, embrittlement, therm. conductivity
high therm. load: ~150 kW at 2 mA, up to 380 oC
 assuming therm. conductivity unchanged
volume swelling?
There is a risk of failure after removal and reinstallation
 good preparation, precautions and safety procedures necessary
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 11
Current integral onto Target E:
1990-2009: 120.5 Ah
(1990-2012: 147.2 Ah)
absorbed: ~ 10%
Current integral/year at HIPA
KHE2 in 2009
MARS results:
1. tooth of KHE2:
31.2 DPA in average
inside: ~ 180 DPA
note: MCNPX result
~ half of this value
ring
4.2 DPA
0
10
20
60
100
140
180
DPA
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 12
Change of properties with radiation (?)
0.5%/dpa
DPA
volume swelling %
S. Zinkle, Effects of Radiation
on Material, 15th Symposium 1992,p. 813
for fast reactor neutrons
Same effect for irradiation with reactor neutrons and high energetic protons?
0 50 100 150 200
DPA
100
50
0
Pure copper
thermal conductivity
% IACS
D.J. Edwards, J. Nuc. Materials 212 (1994), 404
Swelling:
Thermal conductivity l
Transmutation products reduce l:
here: < 10 % effect (mainly Ni)
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: distribution might be not the same for dcs

## Slide 13
Tube2 with prism-like mirror
Filament lamps
Collimator
Shielding (5cm Pb )
with support for
inspection tool
Tube1 with one deflection mirror
Power
Manipulator
remote controlled mirror
Shielding (5cm Pb )
Inspection tool in the hot cell (fully remote controlled)
laser
Camera
+ laser distance
meter
designed by A. Strinning
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 14
constraint: contact-free!
fully remotely controlled in the hotcell
options:
- photos from inside and outside
via camera and mirror tube1
- opening of the aperture
with 2 laser distance meters
- surface roughness with a
tiltable laser beam
Tube1 with 1 mirror
Digital SLR
Camera
mirror
2 laser distance meter
Tube2 with 2 mirror
Examination with the inspection tool
lead,
5 cm
top part:
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 15
Against contamination:
all wrapped into plastic foil:
closed box with camera and
laser meters,
signal- and control cable in
Against damage:
guiding tube in front of collimator
Preparation at the hotcell ATEC and tests
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 16
Results: KHE2 inside after 19 y. in operation
vertical: 80 - 100 oC (2mA)
main damage at exit
 low energetic particles produce
more damage
- some pieces (1-2 mm height)
seems to peel off
- grey surface
 guess: errosion + dirt
entry
exit
sample:
contains Be-7
400
500
600
2mA p
K
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: heisser durch Ni Blende

## Slide 17
horizontal: 350 - 400 oC (2 mA)
main damage at entry
 higher temperature
- large grey pieces peeling off  dirt?
- seems to reveal grain boundaries
might be grown due to temperature
and irradiation
 no swelling or deformation at slits
entry
exit
OFHC Cu
125 mm
slits
completely
intact !
Results: KHE2 inside after 19 y. in operation
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 18
Most astonishing:
no damage of the surface
between vertical & horizontal,
Possible explanation:
thermal expansion/movement close
to the slits, highest stress
Measurement of the horizontal opening
via 2 laser distance meters:
result: very close to original values
accuracy: 0.5 mm
 no swelling observed
example: DV/V=0.5%/DPA
V=10x10x10mm3, 80 DPA
 Dl = 2 x 1.2 mm
Results: KHE2 inside after 19 y. in operation
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 19
front:
back:
more damage at top & bottom
- aperture in very good shape
- one can see beam profile
Results: KHE2 from outside
sample:
no Be-7 but Ag-110m
400
500
600
K
some black pieces peel off
 „golden“ surface below
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: gold: looks not like Cu, some alloy of Ag, Cu etc?

## Slide 20
New KHE2 inserted in March 2013
Same geometrical design as present collimator
- except for sample plates out of OFHC-Cu and Glidcop (4 mm thick)
590 MeV p
Idea:
after irradiation cutting of samples
with electrical discharge machine (EDM) for
tensile test
electrical resistivity measurement
thermal conductivity measurement
Plates controlled by TC
Glidcop
OFHC-Cu
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: Picture from the back side,
in front: 4 TC

## Slide 21
Inspection of new KHE2 in March 2014 (after 1 y)
Reason:
Check of sample plates
indirectly cooled via contact provided by screws
get quite hot inside: ~ 750 oC
KHE2 is in good shape: clean (except for some carbon from Target E)
entry (vertical)
exit (vertical)
wipe test
contains Be-7
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 22
Problem: some screws from the front sample plates are loose!
one came 4 mm out  4 full turns
Reason: probably vibration from the inlet water tube
Procedure:
- Diaphragm has to be removed by the manipulator
- Tighten with larger clamping momentum (5 instead 3 Nm)
 all done with remote handling
Unexpected observation
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB

## Slide 23
New design for KHE2&3
Larger opening allowed by beam transport calc. with TURTLE: + 25%
increase in transmission: 68 %  71 %
less energy deposit on KHE2&3
New design proposed: DP2
less energy deposit than current design: max. T = 302 oC
PIC
@ 3 mA
beam tilted by 1 mrad:
30 cm
KHE2
KHE3
max. T = 385 oC < 405 oC (temp. limit)
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: 2.5 GeV (ESS): 170 cm stopping range

## Slide 24
CAD Illustration (half tube)
Samples?
If samples in tube survived
tensile test
electrical resistivity measurement
therm. conductivity measurement
a) Sample in SINQ-Target (STIPVI): 2011-2012
filled with Cu und Glidcop + 1 thermocouple
Sample tubes will be taken out in June 2014
Cutting of tube in hot cell (when?)
Setup for remote handling not yet done!
electrical resistivity
therm. conductivity
b) Samples from old KHE2 ?  feasibility study
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Notes: STip samples: n+p: 10 to 50 DPA (with damage cross sections of Konobeeyev

## Slide 25
12. Mai 2014
PSI,
Cu- collimator KHE2 (+ 127 mm Ni diaphragm for beam diagnosis):
150 kW, water cooled, 20 years in operation, heavily irradiated (up to 180 dpa)
Remote handeled inspection: No serious damage but highly activated (up to 500 Sv/h)
Remote handling with exchange flask is routine operation (also for other components)
New KHE2 inserted in 2013, inspected in 2014: loose screws at sample plate
Samples from STIP tube, old KHE2, sample plates:
Behaviour of tensile strength, electr. resistivity and thermal
conductivity not known under high energetic protons
Summary
Daniela Kiselev, Beam losses and collimators in transfer lines, 13-14.5.2014, Lund, ESS AB
Beam dump:
similar design to KHE2

## Slide 26
shielding plate
closed
Al-box against contamination
x
Exchange flask above beam line (p-channel)
40 cm steel
Dose rate has to be < 2 mSv/h,
with KHE2 < 0.15 mSv/h (Tc = 90 d)
“bridge”: platform with positioning sticks
for exchange flask
movable
shielding plate

## Slide 27
Displacement cross section (dcs)
damage cross section:
damage function (no. of displaced atoms):
particle energy
w(ER): recoil spectrum
needs nuclear reaction models
x: thickness of the sample
NV: atomic density (atoms/cm3)
modified Kinchin-Pease m.
= NRT model
(Norgett RobinsonTorrens)
Tdam : damage energy
displacement efficiency k = 0.8
some remarks on uncertainties:
ED in Cu: 18 – 43 eV, choice: 30 eV (for MCNPX, dcs)
k = 0.8: for hard sphere model (Rutherford formula)
compensates for the forward scattering

## Slide 28
DPA calculation
Methods and codes:
Displacement cross section (dcs) from A. Konobeyev (Sept. 2010)
evaluated from several reaction c.s. codes,
accounting for defect efficiency h, h=1 for NRT
MCNPX2.5.0: CEM model and ENDF/B-VI (for n, < 20MeV)
for protons:
- displacement cross section for E = 590 MeV only
 o.k. for 1. section of KHE2 (energy loss in 5 cm Cu: ~120 MeV)
for neutrons:
built-in damage cross sections (Monroe Wechsler and Marvin Barnett)
as flux multipliers
MARS15 (2010):
- energy dependent displacement efficiency: k(ER), in NRT: k = 0.8
k(0.1keV) = 1.4 to k(100keV) = 0.3
- Coulomb interaction, formfactors, photons, muons, electrons
- nice feature of 2-dim. plots showing distributions of DPA (+other quantities)
f(E): fluence (particles/cm2)
sdisp: displacement cross section

## Slide 29
no saturation up to 100 dpa
data are for neutrons only (thermal and fast reactors)
 Not much is known for high energetic protons
0.5%/dpa
Swelling after irradiation with neutrons
80 DPA  ~40 % swelling
S. Zinkle, Effects of Radiation
on Material, 15th Symposium 1992,
p. 813-834

## Slide 30
MCNPX2.5.0 + CEM, A. Konobeyev:
6227 barn 4764 barn
 fair agreement: 30 % deviation
Checks on the MCNPX calculation
- (Old) Experiment at Pirex (PSI): 590 MeV protons on 0.3 mm Cu
1 DPA = 1.5 1020 protons/cm2 (LAHET calculation)
(Singh,Horsewell, ASTM STP 1175, (1993), 1003)
- Calculation: MCNPX2.5.0 + CEM model
0.93 DPA due to protons
0.02 DPA due to neutrons
Comparison of the dcs for 590 MeV p
Comparison of DPA:
 very good agreement!

## Slide 31
Displacement cross sections (dcs)
A. Konobeyev:
- E > 150 MeV: average of Bertini, Isabel, INCL4
- 20 < E < 150 MeV: CEM, DISCA code
- E < 20 MeV: ENDF/B-VII (neutrons)
elastic c.s.: optical model + screened Coulomb potential (protons)
E < 28 keV: Molecular Dynamics (MD)
E > 28 keV: Binary Collision Approximation (BCA)
 number of stable defects obtained with the IOTA code (ion-ion collisions)
see U. Fischer‘s talk
for details

## Slide 32
Comparison of results from MCNPX, dcs, MARS
DPA for 1. tooth: Comparison
NRT(MCNPX) NRT(dcs) MD(dcs) MARS
protons: 11.6 8.2 4.8
neutrons: 5.4 5.2 2.3
Total: 17.0 13.2 7.1 31.2
p
1 2 3 4 5 6
tooth
ring
irradiation from 1991 – 2009
Notes: MARS/NRT(dcs) = 5 for 3. ring
NRT(dcs)/MD(dcs) = 2 for 3. ring

## Slide 33
Impurities due to transmutation
(original) material composition for OFHC Cu: 28 ppm impurities
after irradiation: 0.16 w% = 0.015 g
Ni: 0.09 w%
Fe: 0.02 w%
Zn: 0.009 w%
others: ~10-3 w% or less
contribution to electr. resistivity
1.22 mW cm/w%
?
0.27 mW cm/w%
values from
Edwards et al.
valid for < 10 w%
 Ni: 0.11 mW cm, Zn: 0.0025 mW cm
Cu: 1.68 mW cm  < 10 % increase of electr. resistance
This is only the effect due to impurities,
not due to defects in the Cu-matrix.

## Slide 34
water velocitv [m/s]
1 2 3 4 5 6 7 8
max. temperature [K]
The correlation between maximum temperature and water speed becomes weak for velocities larger than 5 m/s, where turbulent flow is fully developed.

## Slide 35
Franz-Wiedemann Law: l = L T s, L = 2.44 10-8 WW/K2
Degradation of phys. properties with radiation
due to (therm.) neutron radiation
 probably not comparable
Behavior at high energetic proton
irradiation not known
Electrical conductivity s
 also thermal conductivity l decreases
Notes: L = Lorenz number

## Slide 36
Was passiert bei hohen Temperaturen?
DK: Korngrösse
HB: Härte
A: Bruchdehnung
Rm: Zugfestigkeit
ab 600 oC starkes Kornwachstum
 diesen Bereich unbedingt vermeiden!
Notes: Als Zeitdehngrenze (Formelzeichen: Rp) wird die Spannung bezeichnet, die bei einer vorher festgelegten Temperatur und Beanspruchungsdauer zu einer bestimmten plastischen Dehnung führt.