## Slide 1: 10B based thin films for next generation of neutron detectors using different deposition techniques
Mewlude Imam1,2, Carina Höglund1,2, Jens Birch1,
Richard Hall-Wilton2 , and Henrik Pedersen1
1Department of Physics, Chemistry and Biology Linköping University (LiU), Linköping, Sweden
2European Spallation Source (ESS) Lund, Sweden
Notes: - Center the title
- ”for the next generation”

## Slide 2: European Spallation Source (ESS)
ESS in Lund, Sweden - the world’s leading neutron source for the study of materials
Neutron detectors based on the isotope 10B instead of 3He
The first neutrons and 7 instruments will be produced in 2019, the full baseline suit of 22 instruments in 2025
Notes: - For “the study of materials”

## Slide 3
Neutron detection using 10B
10B has slightly less neutron absorption cross section compared to 3He
10B + n → 7Li + a + g (94 %)
10B + n → 7Li + a (6 %)
natB contains 80 at.% 11B 20 at.% 10B
Incident neutron
CF4 gas
10B
7Li
a
Substrate

## Slide 4: Boron containing thin film B4C
Elemental B:
- Bad oxidation resistance
- Poor electrical conductivity
B4C:
- Excellent wear resistance, thermally and chemically stable
- Better electrical conductivity
- Easy to deposit with DC magnetron sputtering

## Slide 5: Demands on the thin films
  Thickness > 1 µm
  1- or 2-side coated substrates (neutron transparent)
  Good adhesion and low stress
  No demands on the crystallinity
  High density
  Minimal amount of impurities
Notes: We want as High density as the bulk density. crystilline B4C is 2.52g/cm3

## Slide 6: Deposition techniques in this project
Thermally activated CVD
DC magnetron sputtering
Plasma enhanced CVD
(PECVD)

## Slide 7
DC magnetron sputtering of 10B4C (PVD)
Deposition in an industrial system, CemeCon CC800/9
LiU deposition system

## Slide 8
Required property | Result | OK?
Good adhesion | > 1 mm on Al, Si, Al2O3, etc | 
Low residual stress | 0.09 GPa at 1 mm 10B4C | 
High density | 2.45 g/cm3, 97% of bulk* | 
High 10B content | 79.3 at.% of 10B | 
Low impurities | H +N + O only ~1 at.% | 
Patent SE 535 805 C2
C. Höglund et al., J. APPL. Phys. 111, 104908 (2012)
*O. Knotek et al. Surf. Coat. Tech. 1997, 91, 167
Coatings for different prototype
SEM cross sectional image
Film composition-ERDA
Coatings on Al blades
10B4C
Si
1 mm

## Slide 9: ESS coating facility in Linköping
9/2013: New deposition system ordered - Only for 10B4C coating for neutron detectors - Covers needs of the ESS (6000 m2)
4/2014: FAT documents signed
23 June-2014 - delivery date
2014-2016: Up-scaling - 1000 m2/year
Staff:
1 engineer – 1 September start
1 technician (Q4, 2014)
Carina Höglund ~50%
LiU
”ESS”
Close collaboration with LiU:
Research & competence
- Sputtering, CVD, PECVD, …
Characterization -SEM, SIMS, XRD, ERDA,…
Upgraded LiU deposition system - Backup system
8
Notes: Factory acceptance test

## Slide 10: Demonstrator - IN5 segment
Collaboration ESS – LiU – ILL
0.8 x 3 m2 detector area
25 000 blades with 10B4C, 103 m2 in 45 days (up to 3.3 m2/day)
0.75, 1 and 1,5 mm 10B4C coatings + 1 without coating
50% Ni-plated / 50% low-a Al
Mass production test!
Deadline September 2014
After this: Full scale detector!
9
Notes: 30 um Ni coating on Al blade
See Mathieu Ferraton's talk for more details
Natural Al contains U (uranium) and Th (thorium)

## Slide 11: Deposition using CVD
Expected less stress in the films – less problems with adhesion
Not line of sight deposition –detector parts can be coated assembled, also allows for more complex detector geometries
It is possible to get different film stoichiometry, i.e., BxC where x > 4
Notes: Less stress in the film then sputtering.

## Slide 12: Traditional BxC CVD
Thermally activated CVD, 900-1300 °C Al melts at 660 oC
Boron precursor BCl3/BBr3, produces HCl
Carbon precursor: Light hydrocarbons
typically CH4 passive below 800 oC
Any alternatives?
U. Jansson, J-O. Carlsson, Thin Solid Films 124 p. 101 (1985).
L. G. Vandenbulcke, Ind. Eng. Chem. Prod. Res. Dev. 24 p. 568 (1985).
U. Jansson et al.Thin Solid Films 172 p. 81 (1989).
H. Vincent et al. Carbon 34 p. 1041 (1996).
J. Berjonneau et al. J. Electrochem. Soc. 153 p. C795 (2006).
Y. Liu et al. Appl. Surf. Sci. 255 p. 5729 (2009).

## Slide 13: Alternative CVD route
Organoboranes, i.e. molecules with one or more B-C bonds:
Triethylborane (TEB) B(C2H3)3
Trimethylborane (TMB) B(CH3)3
Tributyl borane (TBB) B(C4H9)3
Very reactive – lower process temperature
Contain both B and C, no Cl
TEB reported to be the best choice for low temperature boron-carbon films *
Available as 10B enriched
TEB - TriEthylBoron
* J. S. Lewis et al. Mater. Lett. 27 p. 327 (1996)
B
H
C

## Slide 14: Thermally activated CVD
Growth parameters:
T = 400 – 600 °C
Pressure 50 mbar
Insulation
Susceptor
Quartz tube
RF Coil
Carrier gas (H2 or Ar)
TEB

## Slide 15: Deposited films
The films were found to be XRD amorphous, regardless of temperature and ambient
Deposition rate at 600 oC: 0.4 µm/h in H2 ambient, 1 µm/h in Ar
Films with thickness of 0.5-1 µm adhere well to both Al blades and single crystal Si (100) surface
H. Pedersen et al. Chem. Vapor Deposition 18 p. 221 (2012)
14

## Slide 16: Elemental composition & density
H. Pedersen et al. Chem. Vapor Deposition 18 p. 221 (2012)
Bulk density for crystalline B4C: 2.52 g/cm3
O. Knotek et al. Surf. Coat. Tech. 1997, 91, 167
Suggested chemical reaction mechanism:
In hydrogen ambient:
At low temperature TEB decomposed BH3 and CH4 -> high B/C
At high temperature TEB decomposed BH3 and C2H4 -> lower B/C
In argon ambient:
TEB only decomposed to BH3 and C2H4
Elastic Recoil Detection Analysis (ERDA)

## Slide 17: Deposition at high T using thermal CVD
Si (100) substrate
Deposition temperature:
700-1200 oC
Good adhesion & dense film
Deposition rate: 1.39 μm/h in hydrogen 955 nm/h in argon ambient at 700 oC
Film density varies in 2.40 - 2.69 g/cm3
BxC deposited at 800 °C in Ar

## Slide 18
B/C = 4.5 at 700 oC with 2.42 g/cm3
T > 1000 oC, mainly deposited C in H2 ambient
H < 0.3 at .%
Precursor: B(C2H3)3 (TEB)
Pressure: 50 mbar
Temperature: 700-1200 oC
Carrier gases: H2 & Ar
Elemental composition by ERDA
Notes: Different T in hydrogen and index peaks, check O, N from ERDA make sure if the impurity level is less than 0.1 at.%

## Slide 19
Hardness (Nano-indentation)
X-ray diffraction
T ≤ 1000 oC, films are amorphous
> 1000 oC graphite in H2 ambient
Hardness 35 GPa and 33 GPa in Ar and H2 ambient, respectively
Structural and mechanical properties

## Slide 20: Plasma Enhanced CVD
Growth parameters:
Pressure 0.2 mbar
No intentional heating
Ar carrier gas/plasma gas
TMB
10B enriched TMB is commercially available
Usually first choice for low temperature CVD
Notes: The reason why we used TMB,

## Slide 21: Early results from PECVD
Highest Deposition rate ~300 nm/h
Smooth and dense films
Film density: 1.25 - 1.49 g/cm3
Notes: Images white color numbers

## Slide 22: Film composition (ERDA)
Deposition parameter:
TMB 5 sccm
Ar 42 sccm
Power 2000 W
composition | Relative amount
B | 38 at. %
C | 41.1 at. %
H | 6.0 at. %
O | 14.8 at. %
B/C=1

## Slide 23: Conclusions
10B containing thin film based detectors – an alternative to 3He detectors
10B4C thin films deposited by PVD, up to 3.3 m2/day, dedicated machine will be around within a month
Thermal CVD process of BxC using TEB shows:
B/C ~ 4.6, impurity level ~ 4 at.% at 600oC
B/C= 4.3, impurity level ~ 0.1 at.% at 700 oC
PECVD using TMB shows promising early results and is under development
Notes: Think it again

## Slide 24: Acknowledgements

## Slide 25
Mewlude.imam@esss.se
yimma@ifm.liu.se
Thank you for your attention!