## Slide 1
Multi-Blade detector update
Francesco Piscitelli
IKON20
2021/02/16

## Slide 2
August 2015
TARGET
ESTIA
FREIA
Multi-Blade
Boron-10-based detector
Reflectometers

## Slide 3
wires
neutrons
strips
10B4C
5∘
A unit
sample
Many units
…
Principle
10B4C
Multi-Blade
flight tube
detector
user
detector arm
sample rotation axis
incoming
neutrons
sample
environment
cathode strips
anode wires
U-frame
Ti-blade
A unit
10B4C coated Ti-blade by the
ESS Coating facility (Linköping)
cathode strips
Assembly at the ESS workshop (Utgård, Lund)
substrate
48-unit detector
Estia

## Slide 4
MB300L
MB18
260mm
130mm
6-unit full length detector
9-unit detector
(half length)
Estia and FREIA
use the same 260mm units:
48 for Estia, 32 for FREIA
48-unit detector

## Slide 5
Multi-Blade: TOOLING is complete and tested on MB300L
cathode strips
parts
A unit
6-unit detector
Gluing machine KV-1
Wiring machine K-7
Oven clamp

## Slide 6
MB300L
MB18
MB18 permanently installed at AMOR since Sept 2020 for the commissioning of the beam line and for friendly user operations.
The AMOR reflectometer (PSI) uses the same principle of neutron focusing guides as Estia.
MB300L Tested at AMOR twice (Sept and Dec 2020)
Many thanks to
Jochen Stahn
for the support

## Slide 7
MB300L Tested at AMOR twice (Sept and Dec 2020)
All aspects matching the requirements and scientific measurements performed
wires X
substrate
neutrons
θ
strips Y
10B4C
A cassette (unit)
Some scattering happening at the PCB below the edge
Apart …

## Slide 8
5.0∘
Centre of blade
4.0∘
5.75∘
5.0∘
5.5∘
Explicitly wrong lower incl.
1 deg off
Nominal
Explicitly wrong higher inclination
Still no clear evidence that this effect will cause a visible
effect on the scientific output of a measurement

## Slide 9
wires X
substrate
neutrons
θ
strips Y
10B4C
A cassette (unit)
Solution 1: GdOx at edge
Solution 2: Blades edge at 2.5deg instead of 5deg
5.0∘
5.0∘
2.5∘

## Slide 10
3 blades with GdOx
GdOx at edge
GdOx

## Slide 11
MB300L Tested again in Dec 2020 (REMOTELY from Utgard)

## Slide 12
wires X
substrate
neutrons
θ
strips Y
10B4C
A cassette (unit)
Solution 1: GdOx at edge
Solution 2: Blades edge at 2.5deg instead of 5deg
5.0∘
5.0∘
2.5∘
X

## Slide 13
Solution 2: Blades edge at 2.5deg instead of 5deg
2.5∘
Ti
Ti
Ti
To be tested at PSI, AMOR, Apr/May 2021.
We are very confident that this solution will optimize the design.

## Slide 15
Off-specular scattering from Fe/Si neutron supermirror
Yoneda wings
Yoneda wings
Sample Horizon
Supermirror edge
(m=3.8)
Supermirror
edge
(from SuperADAM at ILL)
G. Mauri et al., Neutron reflectometry with the Multi-Blade 10B-based detector, Proc. R. Soc. A 474: 20180266 (2018).
Si edge
Correlated
roughness
domains
Spin-flip scattering
signal

## Slide 16
MB18 permanently installed at AMOR since Sept 2020 for the commissioning of the beam line and for friendly user operations.
The AMOR reflectometer (PSI) uses the same principle of neutron focusing guides as Estia.
ESTIA Instrument Proposal
NiTi Multilayer
(q,l)
1
1
2
3
4
5
4
3
2
Measured with Multi-Blade
@ AMOR (PSI)
Simulated
0.065Å-1
0.065Å-1

## Slide 17
Great interest in having a permanent
Multi-Blade detector for AMOR (PSI) by 2022.
Beneficial for ESS
OPPORTUNITY
An Estia before Estia:
Full data chain with the ESS system
Estia commissioning straight forward
Debugging on all systems beforehand
Beneficial for PSI
Best resolution, best rate capability detector for Reflectometry
Many thanks to
Jochen Stahn
for the support

## Slide 18
efficiency | 44% @ 2.5 Å 57% @ 4. Å 82% @ 12 Å
spatial resolution | 0.5 x 3.5 mm2
uniformity | ±1.5%
stability | 2% (over days)
counting rate capability (peak rate) | >3.5 kHz/mm2 (lower limit) >60kHz / 30mm2 (lower limit)
gamma-ray sensitivity | < 10-7 (with 100keV threshold)
fast neutron sensitivity | < 10-5 (with 100keV threshold)
gas gain | 60
overlap | 50% eff. drop in 0.5mm gap
Matching ESS requirements
x3 better than state-of-the-art
>20 better than state-of-the-art
G. Mauri et al., The Multi-Blade Boron-10-based neutron detector performance using a focusing reflectometer, JINST 15, P03010 (2020).
F. Piscitelli et al., Characterization of the Multi-Blade 10B-based detector at the CRISP reflectometer at ISIS, JINST 13 P05009 (2018).
G. Mauri et al., Neutron reflectometry with the Multi-Blade 10B-based detector, Proc. R. Soc. A 474: 20180266 (2018).
G. Mauri et al., Fast neutron sensitivity of neutron detectors based on boron-10 converter layers. JINST 13 P03004 (2018).
F. Piscitelli et al., The Multi-Blade Boron-10-based Neutron Detector for high intensity Neutron Reflectometry at ESS, JINST 12 P03013 (2017).
F. Piscitelli et al. Study of a high spatial resolution 10B-based thermal neutron detector for neutron reflectometry: the Multi-Blade prototype, JINST 9 P03007 (2014).
Multi-Blade characterization
x100 better than state-of-the-art
as good as state-of-the-art

## Slide 19
Multi_blade detector
G. Mauri et al., The Multi-Blade Boron-10-based neutron detector performance using a focusing reflectometer, JINST 15, P03010 (2020) (arxiv: 2001:02965).
F. Piscitelli et al., Characterization of the Multi-Blade 10B-based detector at the CRISP reflectometer at ISIS, JINST 13 P05009 (2018) (arxiv: 1803.09589)
G. Mauri et al., Neutron reflectometry with the Multi-Blade 10B-based detector, Proc. R. Soc A 474: 20180266 (2018) (arxiv: 1804.03962).
G. Mauri et al., Fast neutron sensitivity of neutron detectors based on boron-10 converter layers, JINST 13 P03004 (2018) (arxiv: 1712.05614).
F. Piscitelli et al., The Multi-Blade Boron-10-based Neutron Detector for high intensity Neutron Reflectometry at ESS, JINST 12 P03013 (2017) (arxiv: 1701.07623).
F. Piscitelli et al., Neutron reflectometry on highly absorbing films and its application to 10B4C-based neutron detectors, Proc. R. Soc. A 472, Issue 2185 (2016) (arxiv: 1510.01085v1).
F. Piscitelli et al. Study of a high spatial resolution 10B-based thermal neutron detector for neutron reflectometry: the Multi-Blade prototype, JINST 9 P03007 (2014) (arxiv: 1312.2473).
F. Piscitelli and P. Van Esch, Analytical modeling of thin film neutron converters and its application to thermal neutron gas detectors, JINST 8 P04020 (2013) (arxiv: 1302.3153).
References
Gamma-ray sensitivity
A. Khaplanov et al., Investigation of gamma-ray sensitivity of neutron detectors based on thin converter films, JINST 8 P10025 (2013) (arxiv: 1306:6247).
F. Piscitelli et al., The Multi-Blade Boron-10-based Neutron Detector for high intensity Neutron Reflectometry at ESS, JINST 12 P03013 (2017) (arxiv: 1701.07623).
Fast neutron sensitivity
F. Piscitelli et al., Verification of He-3 proportional counters fast neutron sensitivity through a comparison with He-4 detectors, EPJ Plus 135, 577 (2020) (arxiv: 2002.08153).
G. Mauri et al., Fast neutron sensitivity for 3He detectors and comparison with Boron-10 based neutron detectors, EPJ TI 6, no. 1, p. 3, (2019) (arxiv: 1902:09870).
G. Mauri et al., Fast neutron sensitivity of neutron detectors based on Boron-10 converter layers, JINST 13 P03004 (2018) (arxiv: 1712.05614).

## Slide 20
2D image of the detector (X,Y)
detector Y vs ToF
NiTi Multilayer Multi-Blade data
We are starting construction imminently!