## Slide 1: High entropy alloys – magnetism and neutron diffraction
Johan Cedervall
johan.cedervall@mmk.su.se

## Slide 2: Those who did the work
Dennis Karlsson
Simon R. Larsen

## Slide 3: High entropy alloys
HEAs known for simple structure
Solid solution – i.e. randomly dispersed atoms
Often include a large amount of magnetic elements
Entropy stabilized
Can tune lattice type with Valence Electron Concentration (VEC)
P. Koželj et al., Physical Review Letters 113 (2014) 107001.
D.B. Miracle, O.N. Senkov, Acta Materialia 122 (2017) 448-511.

## Slide 4: AlCoCrFeNi
High entropy alloy?
  Dependent on synthesis conditions
    Gas atomisation
    Arc melting
  B2/bcc structures
Narrow single phase regions
  Spinodal decomposition
Additions of Mn changes the magnetic behaviour
D. Karlsson et al., Additive Manufacturing 27 (2019) 72–79.

## Slide 5: AlCoCrFeNi
bcc vs. B2-phases
Body centered
  Im-3m
Primitive cubic
  Pm-3m
Similar but not identical diffraction patterns
  Structure form factors

## Slide 6: AlCoCrFeNi
Gas atomisation
2 regions with different composition
  Dendritic core (DC)
  Interdendritic (ID)
Both displays the forbidden 100 reflection  B2 structure
Induction melting
Two separate phases
  bcc
  B2
D. Karlsson et al., Journal of Alloys and Compounds 784 (2019) 195-203

## Slide 7: AlCoCrFeMnxNi
Mn additions with changes the bcc/B2 phase mixture
Microstructure is similar to AlCoCrFeNi synthesised with induction melting

## Slide 8: AlCoCrFeMnxNi
Magnetic transition temperature decreases with additions of Mn
The saturated magnetic moment increases with increasing Mn-content
Small difference in magnetic saturation for the gas atomised samples
Big difference in thermal magnetic behaviour

## Slide 9: AlCoCrFeMnxNi
Applications in magnetic refrigeration?
  Magnetic transition at RT
  Large response to a small magnetic field
  Big change in magnetic entropy upon magnetisation

## Slide 10: AlCoCrFeMnxNi
Differential scanning calorimetry
Phase transition temperature decreases with Mn-content
  Similar to magnetometry
Phase decomposition to σ- and fcc phases upon heating

## Slide 11: AlCoCrFeNi - In-situ diffraction
Atomised powder
B2  σ + fcc
Heating rates
  NPD: 1 h measuring time for each temperature
  SXRD: 10 K/min

## Slide 12: AlCoCrFeNi – atomic occupancies
Joint refinements of XRD and NPD patterns
Pure B2 phase
Different site occupancies

## Slide 13: Conclusions
High entropy alloys are not the best way to describe AlCoCrFeMnxNi given the small single phase region
B2 and bcc competing phases when syntesised from melt
  Cooling rate dependant
Soft magnetic, with increasing Msat with increasing Mn-content
Irreversible magnetic thermal effects due to decomposition of the alloys
Specific elemental site occupation in the B2 structure
D. Karlsson et al., Additive Manufacturing 27 (2019) 72–79.

## Slide 14: Acknowledgements
Simon R. Larsen
Dennis Karlsson
Daniel Hedlund
Henry Stopfel
Peter Svedlindh
Lars Riekehr
Ulf Jansson
Peter Harlin
Christian K. Christensen
Jo-Chi Tseng
Premysl Beran
Thomas Hansen