## Slide 1
Electropolishing for SPL cavities
L. Ferreira
TE-VSC-SCC

## Slide 2
OUTLINE
  CERN Niobium electropolishing set-up
  SPL #1
    Measured data from SPL #1
    Crosscheck with data from simulation (SPL #1)
    SPL #2
    New cathode and working procedure
    Measured data from SPL #2

## Slide 3
CERN Nb electropolishing set-up
- Vertical electropolishing (& no rotating parts)
Touch screen control panel

## Slide 4
Polishing speed fit between simulation and wall thickness data
Chart: Polishing speed (µm/h)
Equator | 240.12 | 240.12
Equator | 453.36 | 453.36
Equator | 666.6 | 666.6
Equator | 879.85 | 879.85
Equator | 1093.1 | 1093.1
Iris | 346.74 | 346.74
Iris | 559.97 | 559.97
Iris | 773.23 | 773.23
Iris | 986.42 | 986.42
Chart: Polishing speed (µm/h)
Equator | 240.12 | 240.12
Equator | 453.36 | 453.36
Equator | 666.6 | 666.6
Equator | 879.85 | 879.85
Equator | 1093.1 | 1093.1
Iris | 346.74 | 346.74
Iris | 559.97 | 559.97
Iris | 773.23 | 773.23
Iris | 986.42 | 986.42
Simulation
SPL #1
Wall thickness data
Notes: Reverse engineering

## Slide 5
SPL #1
7.2 µm/h
6.9 µm/h

## Slide 6
Bath temperature & speed vs polishing speed
Chart: Temperature / K
| 281.14999999999998 | 283.14999999999998 | 288.14999999999998 | 298.14999999999998
0 m/s | 2.9253 | 4.179 | 7.5221 | 14.2085
0.018 m/s | 8.3579 | 11.7011 | 17.5516 | 32.178
0.072 m/s | 16.1308 | 19.7247 | 27.2468 | 45.885
0.145 m/s | 21.7306 | 25.0738 | 32.6795 | 57.2518

## Slide 7
Direction of flow
Chart: Velocity profile on z direction
SPL #1

## Slide 8
Surface finishing on SPL #1
SPL #1 cell after 200 µm: bright but grooves and pinholes
Top-Down

## Slide 9
Origin of lines and pits
Origin of grooves
Origin of pinholes
Surface finishing on SPL #1

## Slide 10
Chart: Velocity profile on r direction
Direction of flow
Surface finishing on SPL #1
Notes: Only use 1,3,5mm curves, colour graph, scale for cavity shape.
Nice way to identify radial flow

## Slide 11
SPL #2
New Cathode:
Reduce cathode section:
  Decrease bath speed at the iris.
Promote flow uniformity (less vortex):
  Allow hydrogen to flow preferentially upwards.
Restrict the hydrogen path:
  Avoid or at least hinder the amount of hydrogen that reaches the cavity wall.

## Slide 12
SPL #2
Old Cathode
New Cathode
Reduce cathode section: Hollow cathode
Promote flow uniformity (less vortex): Simple geometry and free flow.
- Restrict the hydrogen path: PFE membrane (70 µm).

## Slide 13
SPL #2
Chart: Velocity profile on z direction
Chart: Velocity profile on z direction
Old cathode
New cathode
Decrease bath speed at the iris

## Slide 14
SPL #2
Old cathode
New cathode
Chart: Velocity profile on r direction
Chart: Velocity profile on r direction
Less vortex

## Slide 15
Chart: Electropolishing process data
| 0.4513888888888889 | 0.45833333333333331 | 0.46527777777777801 | 0.47222222222222199 | 0.47916666666666702 | 0.48611111111111099 | 0.49305555555555503 | 0.5 | 0.50694444444444398 | 0.51388888888888895 | 0.52083333333333304 | 0.52777777777777701 | 0.53472222222222199 | 0.54166666666666596 | 0.54861111111111105 | 0.55555555555555602
10.03.2015 | 130 | 131 | 137 | 135 | 130 | 136 | 134 | 128 | 131 | 135 | 132 | 128 | 126 | 126 | 126 | 126
12.03.2015 | 126 | 137 | 130 | 136 | 131 | 141 | 127 | 138 | 129 | 139 | 125 | 130 | 123 | 126 | 122 | 122 | 122 | 122
10.03.2015 | 12.03.2015
11 µm | 24 µm
Measured data from SPL #2
10 to 15 lpm
Tavg = 7.6 °C

## Slide 16
Measured data from SPL #2
 | Top half-cell | Bottom half-cell
10.03.2015 |  | 
12.03.2015 |  | 

## Slide 17
Questions?