## Slide 1: Monolithic mesophase polymer membrane templated from ternary hexagonal lyotropic liquid crystal system
PhD Candidate: Guang WANG
Supervisors: Lingxue Kong (Deakin University)
Chris Garvey (ANSTO)
Maria Forsyth (Deakin University)

## Slide 2: Background of my PhD project

## Slide 3: Chemicals
Poly(ethylene glycol) diacrylate (PEGDA)
2-Hydroxyethyl methacrylate (HEMA)
Monomers:
Structure directing agent: Dodecyltrimethylammonium bromide (DTAB)
Water
Ratio of DTAB
http://plc.cwru.edu/tutorial/enhanced/files/llc/phase/phase.htm
1,6-Hexanediol diacrylate (HDDA)

## Slide 4: Alignment experiment under electric field
Equilibration
Heating up
Transition temperature
Cooling down
Room temperature
A
B
C
12 h

## Slide 5: Hexagonal LLCs without monomer-Complex viscosity and DSC
Binary system of DTAB and water stable to temperature
σ= 10 Pa, ω=10 rad/s

## Slide 6: Effect of monomers on hexagonal lyotropic liquid crystal mesophase (LLCs)-Polarized light microscopy (PLM)
30℃
70℃
60℃
80℃
80℃
55℃
50℃
30℃
PLM images of ternary system of DTAB, Water and PEGDA
Increasing
Decreasing

## Slide 7
PLM images of ternary system of DTAB, Water and hydrophilic HEMA
25℃
42℃
38℃
35℃
30℃
30℃
35℃
40℃
Effect of monomers on hexagonal (LLCs)-PLM
Increasing
Decreasing

## Slide 8
Effect of monomers on hexagonal LLCs-Complex Viscosity
σ= 10 Pa, ω=10 rad/s

## Slide 9: Effect of monomers on hexagonal LLCs-DSC

## Slide 10: Conclusions
Phase transition temperature (Tt) from hexagonal to isotropic micellar phase observed after adding monomers and Tt varies depend on the monomer and its ratio
Tt Decreased from about 70℃ to about 42 ℃ when PEGDA replaced with HEMA gradually
The transition is reversible
Where Monomer sits
?
Structure retention
Membrane fabrication
Membrane properties

## Slide 11: SLD calculation and contrast variation
Contrast variation |  |  | 
D2O ratio | 0 | 8% | 100%
Tail-deuterated DTAB (D25-DTAB) | 0 | 5.3% | 100%
Fully-deuterated DTAB (D34-DTAB) | 0 | 3.2% | 100%
21% for PEGDA
22% for HEMA

## Slide 12: 1D SANS pattern after contrast variation

## Slide 13: Structure factor calculation vs contrast variation

## Slide 14: Gauss fitting and integral peaks
D25-DTAB+ (H2O+D2O)
Wide Bragg peaks
Inaccurate peak structure
factor calculation
Δλ/λ
10%

## Slide 15: Future works:
V1 membrane diffractometer in Germany ( in September )
BILBY in Australia (Proposal submitted)
Longer collimation system to obtain more uniform wavelength
Wavelength resolution within range between 4% and 30%

## Slide 16: Hexagonal Phase
Two dimensional Fourier series
where:
Harper, P. E., D. A. Mannock, et al. (2001). "X-ray diffraction structures of some phosphatidylethanolamine lamellar and inverted hexagonal phases." Biophysical Journal 81: 2693-2706.

## Slide 17
Thanks for your attention
Suggestions appreciated