## Slide 1: Machine learning, digital twins and atomistic simulations for t-o-f INS
Olivier Delaire a, Aiden Sable a, Xing He a, Bander Linjawi a, Andrei Savici b, Jiao Lin b, Fahima Islam b, Garrett Granroth b, Daniel Pajerowski b, Douglas Abernathy b
aDuke University, Durham NC, USA ,
bOak Ridge National Laboratory, Oak Ridge TN, USA
DTU Mcstas workshop July 2025

## Slide 2
Funding: DOE Office of Science, Basic Energy Sciences
National Science Foundation,
Duke Energy Initiative
Ph.D.
students
Argonne National
Laboratory
Acknowledgements
  Argonne National Lab: M. Krogstad, R. Osborn, S. Rosenkranz, D.-Y. Chung, Z. Hood, A. Said, A. Alatas,
  Oak Ridge National Lab: D.M. Pajerowski, D.L. Abernathy, T. Hong, F. Ye, Y, Liu, S. Chi, L. Boatner, J. Lin, A. Savici
  Ross Stewart (ISIS); Fanni Juranyi (PSI)
  W. Zeier (U. Münster); L. Nazar (U. Waterloo);
  M. Kanatzidis (Northwestern); Hui Wang (Louisville)
  Jie Ma (Shanghai Jiao Tong); Qingyong Ren (CSNS)
J. Niedziela
D. Bansal
Bander Linjawi,
Tyler Wilson,
Patrick Postec,
Aiden Sable,
Kevin Clelland,
Tingguang Li,
Wenda Si
Hung-Min Lin
Postdocs
Niuchang Ouyang

## Slide 3: Spectra beyond phonon quasiparticles
harmonic phonons: 𝛅 -functions on dispersions
Weakly Perturbed:
damped harmonic oscillators
Lorentzian-like, shifted
E
Q0
Q
E
Q
Q0
Harmonic:
delta functions
)
Strongly Perturbed:
strong renormalization,
complex spectra (eg. satellites),
quasi-elastic from damped fluctuations
E
Q
Q0
E
Q
Q0
Superionics:
Nature Physics 15, 73 (2019)
PNAS 117, 3930 (2020)
PbTe, SnTe:
Nature Materials 10, 614 (2011)
PRL 112, 175501 (2014)
strong disorder and anharmonicity:
  - complex spectral functions
  - no-longer well-defined quasiparticles

## Slide 4: Big data from time-of-flight INS
Energy transfer, E
Wave vector transfer, Q
Dynamical structure factor S(Q,E) in Ge crystal at T=5K from ARCS @ SNS

## Slide 5: pathSQE: workflow overview
BZ [-3 -3 1] Page 3: All M-𝚪 segments
Efficient, Mantid-compatible framework
Data normalization and errors properly handled
Extensive data visualization and coupled simulations
Aiden Sable

## Slide 6: pathSQE: workflow overview
Efficient, Mantid-compatible framework
Data normalization and errors properly handled
Extensive data visualization and coupled simulations
Aiden Sable

## Slide 7: Ge ARCS data processing with pathSQE
Expt.

## Slide 8: INS data processing, comparison with DFT
Single-crystal Ge phonons dataset (INS vs DFT)
DFT
INS
Sim.
Expt.

## Slide 9: Machine learning for lattice dynamics model inversion based on INS data
from INS
(ARCS, folded+padded)
“inverted” from
trained neural net
validation, NN21
Parameterized
Hamiltonian
Card=35 ;
Training data: 50,000 [, I(q,E)] pairs ;
Convol. Neural Net, trained 50 epochs

## Slide 10: VAE model architecture for FC inversion from I(q,E) spectra
VAE dual-objective loss function
FC Reg MSE loss on FC predictions
Note: Grid search optimization identified well-performing hyperparameters:
Nlat = 20, wKLdiv = 1e-6L

## Slide 11: Ongoing work: model inversion on less data
90° rotation, 3 hours
Which orientations to choose?
→ Potential for experiment optimization / steering
ɸ
1° rotation, 2 mins
✅
ɸ
✅
(!)

## Slide 12: Ongoing work: model inversion on less data
ꞷ = 42°
ꞷ = 75°

## Slide 13: ML FC capture experimental dynamics better than DFT FC

## Slide 14: Ongoing work: t-o-f resolution
McVine resolution modeling → intrinsic linewidths, INS deblurring for FC inversion
Quantitative comparisons to simulation results (w/ Niuchang Ouyang)
(w/ Fahima Islam, Garrett Granroth)
ARCS at SNS

## Slide 15
Bi single crystal with 107g mass
Mosaic < 0.27°
INS (CNCS) T=2K, Ei=20meV folded in high symmetry directions (36 BZ in H0L planes)
High-resolution phonon energies and linewidths in bismuth
(H0L) reciprocal plane
Bi: no mass disorder (single isotope)
Purely coherent neutron cross section
Large crystal of high quality
CNCS 20meV data visualization (~6h scan)
[1] Yanell J., et al., IBM Journal of Research and development. 8, 234-240(1964)
Bi INS data from TAS (1964)
Notes: Disperion energy unit

## Slide 16
Comparison between INS and DFT
Bismuth INS intensity for S(Q,E) in good agreement with DFT harmonic simulations (requires including spin-orbit coupling)
(INS at 300K, CNCS, Ei = 12meV)
Notes: Animate the slices

## Slide 17: Monte Carlo resolution for t-o-f INS
McVine resolution modeling → intrinsic linewidths
CNCS at SNS

## Slide 18: Monte Carlo resolution: intrinsic linewidths
McVine resolution modeling → intrinsic linewidths
Quantitative comparison to simulations of linewidths from anharmonic scattering

## Slide 19
First-principles simulations including finite temperature and disorder: AIMD and MLMD
Gordon Bell Prize 2020
Phys. Chem. Chem. Phys., 2022, 24, 18361
J. Chem. Phys. 159, 054801 (2023)
https://doi.org/10.1063/5.0155600
Additional ML surrogate potentials:
Neuro-evolution potential
https://gpumd.org/
Gaussian approximation potential
https://github.com/libatoms/QUIP
Moment tensor potential
https://mlip.skoltech.ru/download/

## Slide 20: ML for materials simulations: MLIPs
DeePMD neural net potential trained on VASP AIMD
AIMD trajectories at set of T’s
MD in LAMMPS

## Slide 21
MLMD: predict S(Q,E) including full anharmonicity
Strong phonon broadening starting at low T, hope to check with CNCS / AMATERAS
50K
150K
300K
450K
600K
phonon broadening in Cu argyrodite

## Slide 22: Liquid-like dynamics in crystalline Li6PS5Cl
Excess spectral weight on warming reveals Li+ stochastic motions at low frequency
(similar to INM’s in liquids)
DOS shape, vs , evolves from quadratic (solid-like) to linear (liquid-like)
Nature Physics 21, 118 (2025)

## Slide 23: Comparing QENS measurements and MLMD simulations
QENS
vs
MLMD
Chudley-Elliot fits of measured and simulated QENS spectrum
Measured and simulated QENS spectrum
Nanosecond duration MD trajectories → match BASIS resolution (~3.5meV)

## Slide 24: Subset of ML Force Fields from Materials Project
https://matbench-discovery.materialsproject.org/

## Slide 25: Ge dispersion from 14 MLFFs
DFT Results

## Slide 26: FC domain from ensemble of universal MLFFs

## Slide 27: Conclusions
ToF INS resolution needs to be systematically simulated to correct measured excitation linewidths
4D ToF INS datasets can benefit from folding and automated slicing (ideally updated with live events)
AI/ML can transform experimental and simulation workflows
Need AI to steer experiments and inform/refine sample models
Many exciting opportunities to work together!

## Slide 28: Extra Slides

## Slide 29: Simulation inference and latent space analysis

## Slide 30: Reconstructions are accurate across simulated test set
Most dissimilar test spectra to assess performance across FC phase space
Input
Recon.
Input
Recon.
Input
Recon.

## Slide 31: 15k-D spectra are accurately represented with 11-D encodings

## Slide 32: High-fidelity FC predictions on simulated test data

## Slide 33: Active latents nonlinearly encode to underlying FC
Mutual Information: a non-linear measure of the statistical dependence between two random variables
Difference between the entropy of one variable and its conditional entropy given the other variable.
Entropy: uncertainty or randomness of a random variable
Conditional Entropy: uncertainty of one variable given the knowledge of another

## Slide 34: Semantic grouping in latent space mirrors physical interactions
UMAP (Uniform Manifold Approximation and Projection): unsupervised ML for non-linear dimensionality reduction
Known for preserving both local and global structures