## Slide 1: Simulating diffractive optics for neutron techniques
Advanced computer simulations methods for neutron scattering instruments
Mano raj Dhanalakshmi Veeraraj
ICNS 2025

## Slide 2: Fresnel zone plate (FZP)
Refractive index of hard X-rays and cold neutrons are similar n = 1-δ-iβ < 1
Amplitude
zone plate
Fresnel lens
Refractive lens
Phase
zone plate

## Slide 3: Fresnel zone plate (FZP)
Kearney, et al. (1980)
Altissimo, et al. (2004)
Dhanalakshmi Veeraraj, M.r., et al (2025)
Ffzp =
Ffzp ∝
Refractive index of hard X-rays and cold neutrons are similar n = 1-δ-iβ < 1
Neutrons
Highly chromatic
Can be fabricated by e-beam lithography

## Slide 4: SEM images of a Nickel FZP

## Slide 5: Understanding diffraction efficiency
incoming radiation
DT
p
1st order
0th order
-1st order
Diffraction grating
When the duty cycle is 0.5

## Slide 6: FZP fabrication challenges
Quite challenging to get,
  Small outer-zone widths (<100s of nm) AND tall structures (> 2 um)
    High aspect ratio nano structures
  Perfect 50% duty cycle

## Slide 7: Soooo…. Neutron zoneplates
Kearney, et al. (1980)
Altissimo, et al. (2004)
Me 🙋🏻, et al. (2025)

## Slide 8: New improved FZP component
def FZP_simple(rad, dr, bs0rad, sigma_abs, sigma_inc, sigma_coh, rho,thickness, gamma, order, eta):
  Included in McStas 3.5.32
  Nice simple approximation
  Handles efficiency as if it is an absorption FZP
def FZP_mod (rad, dr, bs0rad, sigma_abs, sigma_inc, sigma_coh, rho, thickness, gamma,lambda0):
  Handles efficiency as if it is a binary phase FZP
  Imperfections can be included
  Soon available to public

## Slide 9
Mask
Source_simple
Slit
Slit
Fzp_mod
PSD_monitor
Instrument setup
• Magnification : ~ 7 X
0.88 m
6.6 m
Scheme of a neutron microscope

## Slide 10
Mask
Source_simple
Slit
Slit
Fzp_mod
PSD_monitor
Instrument setup
• Δλ/λ : 0.15
• Magnification : ~ 7 X
0.88 m
6.6 m
Scheme of a neutron microscope
Highly chromatic
Not suitable for broad band imaging
star30.png
Simulated magnified images:

## Slide 11: Is sensitive to duty cycle
Is sensitive to thickness of material
More close to reality

## Slide 13
Mask
Source_simple
Slit
Slit
Fzp_mod
PSD_monitor
Instrument setup
• Δλ/λ : 0.15
• Magnification : ~ 7 X
0.88 m
6.6 m
Scheme of a neutron microscope
Highly chromatic
Not suitable for broad band imaging

## Slide 14: A Neutron Achromat
Suitable as an objective lens imaging with broadband radiation
Hybrid optic by combining individual optics with opposite dispersive power
Kubec, A. et al. (2022)
Sanli, U. T. et al. (2023)
Achromat condition :: Frl= -2* Ffzp
λdesign = 5 Å
Lens aperture = 1.4 mm
Fachromat = 0.8 m
Fequi- FZP = 0.8 m
Simulated data

## Slide 15
300 mm
SEM image of the Diamond CRL
Image of the Diamond CRL
SEM of the Ni FZP
Aspect ratio: 41

## Slide 16: Experimental data: NeXT, ILL
Experimental data
• FAchromat at 5Å : 0.8 m
• Lens aperture : 1.4 mm
• Magnification : 6.67 X
• Exposure time : 60 minutes
• Wavelength : 5 Å
• Δλ/λ : 0.15
• Field of view : 5 mm
• ~20 µm structures resolved
High resolution magnified neutron image
Matches very well with the simulations
🥳😁
We have an achromatic neutron objective lens
McStas was a huge part
Benchmarking
Troubleshooting
Expectation management
0.5 mm

## Slide 17: Thanks for your attention Questions ??? Comments??
300 nm
Laboratory for X-ray Nanoscience and Technologies (LXN), PSI
  Di Qu
  Silas Strebel
  Hui-Yuan Chen
  Peng Qi
  Konstantins Jefimovs
  Joan Vila-Comamala
  Christian David
Laboratory for Neutron Scattering and Imaging, PSI
  Markus Strobl
  Joachim Kohlbrecher, SANS1
  Anders Kaestner, ICON
  Matteo Busi, BOA
Large scale structures, NeXT beamline, ILL
  Alessandro tengattini
  Lukas helfen
  Anna fedrigo