## Slide 1: ESS Medium Beta Cavity Design and Construction in LASA
Saeid Pirani

## Slide 2: OUTLINE
ESS medium-beta section
Recent update and status at LASA
Design parameters of medium-beta prototypes
  Fabrication – Subcomponents frequency control
  Fabrication – Assembly and cavity welding
  Fabrication and Pre-Tuning
Fine grain 6 cell cavity vertical test result

## Slide 3: ESS medium-beta section
MB cavity technical requirements | 
Frequency (MHz) | 704.42
Number of cells | 6
Geometric beta | 0.67
Nominal Acc. Gradient (MV/m) | 16.7
Epeak (MV/m) | < 45
RF peak power (kW) | 1100
Q external | 5.9-8×105
Q0 at nominal gradient | > 5×109
INFN-LASA activities:
Series
In-kind contribution of 36 medium-beta (MB) cavities, including Niobium procurement, Cavity fabrication in the industry, Documentation, Certification activities, Cold test in a qualified infrastructure, Transportation and Man power for the above activities.
Prototypes
Two MB cavity prototypes (same geometry different materials) have been designed, fabricated and will be cold tested at INFN-LASA.

## Slide 4: Recent update and status at LASA
PDR, held in LASA on 19 May 2016, of INFN-designed MB cavity : Approved
Suggestions from PDR review committee
  Study on Multipacting: Complete
  Qext vs Field Flatness: Complete
  Study on HOM shifting with mechanical tolerances: Complete
Prototypes
  Fabrication (Fine Grain (FG) & Large Grain (LG)): Done
  FG cavity vertical test: Done
  LG cavity vertical test : soon

## Slide 5: Design parameters of prototypes
RF Parameters | INFN design | ESS spec.
Riris (mm) | 50 | ≥47
Geometrical beta | 0.67 | 0.67
Frequency (MHz) | 704.42 | 704.42
Acc. length (m) | 0.855 | 0.855
Cell to cell coupling k | 1.55%↗(+26%) | 
π-5π/6 mode sep.(MHz) | 0.70↗(+30%) | >0.45
G (Ω) | 198.8 | 
Optimum beta, βopt | 0.705 | 0.705
Max R/Q at βopt (Ω) | 374 | 
Eacc at βopt (MV/m) | 16.7 | 16.7
Epeak/Eacc | 2.55 ↗ (+7%) | 
Epeak (MV/m) | 42.6 ↘ (-6%) | < 45
Bpeak/Eacc(mT/MV/m) | 4.95 ↗ (+3%) | 
Q0 at nominal gradient | >5×109 | >5×109
Qext | 7.8×105 | 5.9~8×105
  Design goal
Plug-compatible
Larger cell-to-cell coupling factor, k>1.5%
Allowing for a slight modest sacrifice on Epeak and R/Q
Mechanical parameter | INFN Design
Cavity wall thickness (mm) | 4.5
Stiffening ring radius (mm) | 70
Cavity Internal volume (l) | 69
Cavity internal surface (m2) | 1.8
Stiffness (kN/mm) | 1.7
Tuning sensitivity KT (kHz/mm) | -210
Vacuum sensitivity KV for Kext ~ 21 kN/mm (Hz/mbar) | 31
LFD coefficient KL for Kext ~ 21 kN/mm (Hz/(MV/m)2) | -1.7
Plug-compatible

## Slide 6: Fabrication - Subcomponents frequency control and trimming
HC
Dumbbells (DBs) and End groups (EGs) are frequency-controlled before and after trimming
DB trimmed

## Slide 7: Fabrication – Assembly, cavity welding
LG DB
Large grain cavity
Fine Grain Cavity

## Slide 8: Pre-tuning (in air, room temperature, before BCP)
Chart: MB001 Field Profile just After Fabrication
Cavity just fabricated: f=703.51 , FF=70%
Cavity after final tuning: f=703.11MHz, FF=97%
Chart: MB001 Field Profile After Pre-Tuning
Tuning an inner cell
FF=97%
FF=70%

## Slide 9
Fine Grain 6 Cell Cavity
Vertical Test Measurement Results

## Slide 10: Cavity properties
Frequency @ 2K
  704.213 MHz (as expected)
Length @ room temperature
  1257.6 mm
Qext for power coupler antenna @ 2K
  6E9
Qext for pickUp antenna @ 2K
  1.5E11

## Slide 11: Power Rise @ 2K
100 W CW cryo power, i.e. 16,7 MV/m @ Q0 5e9

## Slide 12: Radiation

## Slide 13: Static Lorentz Force Detuning Free cavity
Chart: Kext (kN/mm)
| 0.0001 | 0.0005 | 0.001 | 0.005 | 0.01 | 0.05 | 0.1 | 0.5 | 1.0 | 5.0 | 10.0 | 21.0 | 50.0 | 100.0 | 200.0 | 300.0 | 500.0 | 1000.0 | 2000.0 | 3000.0 | 5000.0 | 10000.0 | 20000.0 | 30000.0 | 50000.0 | 100000.0
Stiffening ring radius = 70 | -14.4851 | -14.482 | -14.478 | -14.4463 | -14.4068 | -14.0992 | -13.7338 | -11.4013 | -9.4489 | -4.282 | -2.7811 | -1.8041 | -1.2202 | -0.99535 | -0.88002 | -0.84114 | -0.80988 | -0.78633 | -0.77453 | -0.77059 | -0.76744 | -0.76508 | -0.76389 | -0.7635 | -0.76318 | -0.76295

## Slide 14
HOM
The monopole mode close to 5th machine line
Directly measured at 2K, F = 1741.8 MHz (>19 MHz from machine line at 1761.05 MHz)
Close to expected value, <1 MHz to simulation at 1742.4 MHz.

## Slide 15
Special thanks to my colleages in LASA-INFN for their frindly and colaborative attitude
Thanks for your attention

## Slide 17: Study on Multipacting
Used FishPact code
For INFN MB cavity, the two-point multipactings are found in small regions near equator (<<1 mm)
First order MP occurs in the Eacc range of 7 MV/m to 14 MV/m, with maximum final impact energies around Eacc = 11 MV/m, 30.2 eV and 33.3 eV for inner cell and end cell, respectively.
Chart: Max final impacting energy after 20 impacts for LASA MB cavity
| 8.0 | 9.0 | 10.0 | 10.5 | 11.0 | 12.0 | 13.0 | 14.0
Inner cell | 8.0233 | 17.9517 | 27.014 | 29.5905 | 30.1015 | 25.1393 | 15.5972 | 7.3291
Pen HC | 2.0842 | 10.4309 | 21.0577 | 29.1858 | 29.575 | 21.9762 | 11.7056 | 4.9487
End HC | 2.0863 | 10.3983 | 20.9352 | 29.3087 | 33.3086 | 21.9513 | 11.7194 | 4.9746
Pen HC/End HC
Typical SEY
# The impact energy for the 1st order two-point MP is in the range of 30 - 50 eV, irrespective of RF frequency.
Although two-point MP’s are ubiquitous, they are not expected to limit the cavity performance owing to the fact that the impact energy is very close to the first cross-over of the secondary emission yield (SEY) curve, which shifts up after the surface is “cleaned up” by processing.
----- R.L. Geng
# Geng, R. L." Proc. of the PAC’2003 (2003): 264-268.

## Slide 18: Study on Qext vs Field Flatness
Chart: Field Flatness
| 0.990113756958537 | 0.921661445243915 | 0.881821026798215 | 0.841545255944803
cells 3,4 stretched | 784385.1381 | 848740.7939 | 885045.7173 | 925807.0828
cells 1,6 squeezed | 941503.8905 | 898310.9145 | 857866.497 | 784385.1381
Chart: Field Flatness
| 0.990113756958537 | 0.803016198100912 | 0.712962618560536 | 0.630276916219379
Cell 1 stretched | 784385.1381 | 611475.1545 | 541880.1169 | 482514.9336
Cell 6 squeezed | 611389.671 | 642639.2181 | 680527.3556 | 784385.1381
Chart: Field Flatness
| 0.834286139922906 | 0.869112386346698 | 0.908179055502731 | 0.990113756958537
cells 3,4 squeezed | 686398.1121 | 706394.5566 | 730609.8641 | 784385.1381
cell 1,6 stretched | 784385.1381 | 718830.4939 | 689329.0813 | 661536.5362
Chart: Field Flatness
| 0.682116578155992 | 0.745824072909241 | 0.818403123325423 | 0.990113756958537
Cell 1 squeezed | 1289964.7436 | 1137854.9905 | 1009091.8525 | 784385.1381
Cell 6 stretched | 784385.1381 | 945529.1717 | 1060909.3345 | 1202169.9147
Four common types of field distribution acchieved by stretching or squeezing cells
With field flatness, FF≥90% the Qext is expected in range 7 to 9 × 105

## Slide 19: Study on Qext with tuning
Since the end cells are not the same as inner ones, stretching or squeezing whole cavity will lead shorter length change on end cells, thereby affecting the frequency and field flatness.
Stretching cavity leads decreasing Qext, while squeezing leads increasing Qext. The sensitivity is about 0.18E+5/mm
1 mm squeezed cavity by Freq. tuner
Chart: Length variation
| -2.0 | -1.0 | 0.0 | 1.0 | 2.0
 | 704.012 | 704.195 | 704.378 | 704.561 | 704.744
Chart: Length variation
| -2.0 | -1.0 | 0.0 | 1.0 | 2.0
 | 749746.5921 | 766262.3764 | 784385.1381 | 802461.5899 | 820423.8976
Cavity tuner effect on frequency and Qext
Length changes on each cell by squeezing the cavity 1 mm
FF trend during squeezing
FF trend during stretching

## Slide 20: Tuning after Bulk BCP
Cavity just fabricated: f=703.51 , FF=70%
Cavity after tuning: f=703.11MHz, FF > 97%