## Slide 1: Luminescent Materials for Proton Beam Imaging
Thomas Shea
Cyrille Thomas
Young Joong Lee
Monika Hartl
And the Luminescent materials collaboration
www.europeanspallationsource.se
26 April, 2017

## Slide 2: Layout
Large Collaboration
Luminescent Coating Development
Planning and Project Schedule

## Slide 3: Large Collaboration Luminescent Coating Development
ESS BI: project lead, support in all areas
ESS Target Division and NSS: Material scientists: advise, environment and material lifetime calculations, R&D luminescent materials
Oslo University: measurements, XRD, low energy proton beam, photo-luminescence, thermal characterization
HV: Develop coating process, prepare samples, industrialisation of process
BNL: BLIP (isotope facility), high energy proton Irradiation test (under RADIATE collaboration)
GSI: heavy ion facility irradiation, expertise in luminescence materials
SNS: high power target, share expertise, common interest
Stony Brook University: coat SNS target, process and material development
Los Alamos National Lab: Post Irradiation exam, XRD, High energy Proton beam
J-Parc: proposed collaboration, low energy ions facility,

## Slide 4: Luminescent Coating Requiremements
The photon yield: predict signal signal intensity and signal to noise ratio and related image quality
The emission spectrum: the photons wavelength (or energy) is of prime importance.
  It should be in an efficient range for the readout image systems
  It should be on a different from the proton beam induced fluorescence of the (residual) gas environment.
The luminescence lifetime: should be less or much less than 1µs in order to perform a still image of the beam on the moving target
Radiation tolerance: the luminescence properties should remain sufficient to permit minimal imaging performance along the life of the coated component
The temperature dependence: the luminescence yield at should be understood. The SNS coating has a strong dependence on temperature, and at 473K its luminescent yield is dramatically reduced
Luminescence from secondary particle: neutron, gamma, and other hadron particles may distort the beam density profile
Mechanical properties: compatibility with the coating process and strength of the coating
Vacuum compatibility: outgassing rate of the material should be acceptable for the vacuum system

## Slide 5: Candidate Materials
SNS material:
  Al2O3:Cr
Additional materials:
  Y2O3: successfully plasma coated (HV)
  Y2WO6: successfully produced (ESS)
  lanthanide doped Y2WO6
  Y2O3:Pr / Y2O3:Ce
  Others

## Slide 6: Luminescent Material Down-Selection Current Status
Ideal Material
∞
0
Radiation Tolerance
∞
0
Luminescence Yield
Temperature dependency
∞
0
Luminescence Lifetime
0
∞
SNS Al2O3:Cr (Not anymore produced)
HV Al2O3:Cr (SNS like)
?
Coating process compatibility
Luminescence Properties
Radiation Tolerance
Industrial Coating process
Y2O3, Y2WO3 and doped materials
More materials in the pipeline
Vacuum Compatible
1
0
Spectrum ≢ gas spectrum
0
1

## Slide 7: SNS material luminescent properties
Spectral measurement on end of life and freshly installed SNS Target
Ruby lines measured and characterised
O lines
He lines
O lines
Investigation on ‘oxygen lines’:
Sharp lines at 777nm and 426nm
Short lifetime (<1µs)
Almost constant intensity along lifetime of the material
Proton and photo emission spectrum comparable
Photo-luminescent and proton-luminescent spectra

## Slide 8: Irradiation with no activation
Structure and composition
Thermal effect on luminescence
lifetime
Degradation from heavy ions
Heavy ion irradiation of SNS coupon at GSI
SNS coupon sample
1012 U -> 1.8 10-3 DPA
0.1 DPA
SNS TIS intensity
0.002 DPA
SNS luminescence vs. dose

## Slide 9: Structure and composition
9
XASF and XEOL
ISIS user labs:
X-ray fluorescence spectroscopy:
Al2O3 95.208 %
P2O5 0.563 %
Cr2O3 3.791 %
Expected Cr3+
Structure: octahedral
“P” might influence the structure formed upon spraying
  Further investigation needed:
  Knowledge to produce precursor powder!
Tools in place for the determination of the structure and composition
XRD (Olso):
Al2O3 -> 2Al + 3/2 O2
XASF performed at MAX II
Reduction to be thought the cause of Oxygen lines observed in the SNS spectrum, supported by literature on luminescent material, but not yet demonstrated

## Slide 10: Oslo Cyclotron Low energy proton beam
OCL proton port
New OCL FC (ESS – Oslo) 19/04/2017
HV coated sample
Fibre coupling lens to spectrometer
Camera view axis
Image of the beam
Current reading
Preliminary result
Consistent with SNS data

## Slide 11: Y2WO6: powder characterisation
Proton luminescence
Photo-luminescence (ESS LED / Oslo Spectrometers)
Image of the proton on pellet sample (OCL)
Powder produced at ESS (Monika Hartl)

## Slide 12: Proposal for Los Alamos Characterization with ESS-like beam
Presented to committee this month for beam time Fall 2017
800 MeV p

## Slide 13: Irradiation Campaign, with activation
Under RADIATE collaboration, coated samples on Al from HV: Al2O3:Cr and Y2O3
  Cassette produced (assembles and sealed 04/04/2017)
  All cassettes passed QA tests and are now allowed to be irradiated
    Critical milestone reached!

## Slide 14: Latest News
Dear Colleagues
I am pleased to inform you that as 6:55 PM the BIG RaDiATE Experiment at BLIP is on with 180 MeV and 140 uA beam on target.
…

## Slide 15
Thank you

## Slide 16: Coating Development Schedule
PDR ✓
CDR
SAR
Mock-up Ready
2019
2020
2018
2017
2016
HiRadMat ✓
Ion beam
TW and PBW Spray
GSI √
SNS Target Coating ✓
SNS Target Coating
PIE (LANL)
TW and PBW Spray
Dump Spray
New Dump/ screens Spray
New TW and PBW Spray
BLIP: cassette ready for irradiation ✓
BLIP Irradiation
Present time

## Slide 17: Imaging Systems Team
Oslo University:
Håvard Gjersdal, Ole Rohne, Martin Jaekel, Erik Adli
ESS:
Cyrille Thomas, Thomas Shea
Monika Hartl, Yong Joong Lee
Collaboration, Coordination
HV:
Shrikant Joshi
Produce Samples
Develop Industrial Process
Coating of the Target, PBW, DumpL
Imaging System
Design
Production
Luminescent Material Coating Development
Qualify Material
Industrial Coating Process

## Slide 18: Down-selection
The down selection process will go through several phases:
Phase 1: Material selection and evaluation of process compatibility:
  Material identification, compatibility with thermal spray, compatibility with mechanical requirements.
Phase 2: Refinement of the deposition process, performance of factory floor testing:
  Sprayed sample and refinement of the coating process, and verification of the photo-luminescence
Phase 3: Photoluminescence Characterisation:
  Photoluminescence study: time resolved and spectra, vacuum compatibility, photoluminescence temperature dependence.
  As complementary studies, and for later irradiation test, the most promising material candidates should also have structural measurements records. This can be done by means of X-ray Diffraction techniques, Neutron Diffraction Techniques, and eventually SEM imaging.
Phase 4: Irradiation with no or minimal activation:
  Proton luminescence yield and spectrum, low energy proton beam, but also at high energy beam.
  Characterise radiation tolerance: thermo-mechanical studies, and luminescence properties
Phase 5: Irradiation with significant activation:
  Irradiation with neutron and protons, aim to mimic radiation environment of ESS
  Qualify the material for high power target after PIE, phases 3 and 4
  Phase 6: Industrialization:
  Final phase: documents the industrialised process for the preparation and coating of the selected material on the TW, the PBW, and the Dump (Dump surface and / or screens)

## Slide 19: Luminescence lifetime
Bench test setup at ESS
D1
D2
Sample
Source
BS
Emission spectrum lifetime:
  Mean decay value 1.15ms
  Too large compared to pulse width (2.8ms)

## Slide 20: Temperature dependency
In-vacuum and in-air setup (ESS Vacuum Group):
Controlled sample heater + Spectrometer
Measure Outgassing
Measure Photon Yield at nominal Target temperature
Thermal: Air and Vacuum
70% drop at 200 C
Proton excitation (OCL)
Found same properties of the photo- proton- emission spectra vs. temperature:
  Large drop photon yield at Target operating temperature: 200 degrees C
Courtesy H. Gjersdal

## Slide 21: Irradiation Campaign
Post Irradiation Examination:
  XRD, TEM, (PNNL) awaiting for confirmation
    XANES, XAS, complementary analysis of the material (BNL, Diamond synchrotron sources, proposal to be submitted in May2017)
  Proton excitation emission spectrum and imaging (LANSCE)
    Proposal submitted, awaiting for confirmation of acceptance and dates for the experiment
      Validation of the coated materials for the ESS target
      Characterisation of the spectrum and eventually oxygen lines and reduction process hypothesis

## Slide 22: New Candidate Material
Preliminary testing: ESS baked powders
  Photoluminescence spectrum (ESS – Oslo)
  Proton Luminescence spectrum (OCL – Oslo cyclotron)
Coating development: method and preparation by HV (S. Joshi - University West)
  Proton spectrum and image
  Irradiation

## Slide 23: Next to come …
Method and preparation for the industrial process for coating the Al2O3:Cr materials
Qualification for the Al2O3:Cr coatings after PIE of the BLIP irradiation campaign:
  Decide which material may be coated on the Target Wheel and Proton Beam Window
Characterisation of the new materials:
  Proton luminescence spectra yield, and spectra at target temperature (200° C)
  Photo-luminescence lifetime
  Irradiation campaign
Method and preparation for the industrial process for coating the new materials, starting with Y2WO6 and lanthanide doped Y2WO6
Develop the combustion gun for in-situ coating of the target