## Slide 1: ESS Cryomodules
Christine Darve
(with input from CNRS-IPNO and CEA-IRFU)
ESS Engineering Lecture
Lund University
September 14, 2017

## Slide 2: Outline
  Cryomodule Functions
  Cryomodule Components
  Cryomodule Assembly
  How to operate a cryomodule

## Slide 3: Main function: to house SRF cavities
Beam
RF Input
Power Amplifier (Klystrons)
Power Coupler
Gap
Waveguide
Lorentz Force
Electrical Field
Magnetic Field
High b - Elliptical cavity
Low b - Spoke cavity
Equivalent circuit for a 4 cell cavity with beam pipe
b= v/c

## Slide 4: ESS Linear Accelerator Layout
Chart: Beam Beta
Spokes
Medium β
High β
DTL
MEBT
RFQ
LEBT
Source
HEBT & Contingency
Target
2.4 m
4.6 m
3.8 m
39 m
56 m
77 m
179 m
75 keV
3.6 MeV
90 MeV
216 MeV
571 MeV
2000 MeV
352.21 MHz
704.42 MHz
 ESS needs high gradient SRF cavities
Notes: 400 m/ 600 m tunnel = SRF

## Slide 5: ESS Requirements and RF Parameters
 | Medium |  | High
Geometrical beta | 0.67 |  | 0.86
Frequency (MHz) | 704.42 |  | 
Number of cells | 6 | 5 | 
Operating temperature (K) | 2 |  | 
Epk max (MV/m) | 45 | 45 | 
Nominal Accelerating gradient (MV/m) | 16.7 | 19.9 | 
Q0 at nominal gradient | > 5e9 |  | 
Qext | 7.5 105 | 7.6 105 | 
Iris diameter (mm) | 94 | 120 | 
Cell to cell coupling k (%) | 1.22 | 1.8 | 
p,5p/6 (or 4p/5) mode sep. (MHz) | 0.54 | 1.2 | 
Epk/Eacc | 2.36 | 2.2 | 
Bpk/Eacc (mT/(MV/m)) | 4.79 | 4.3 | 
Maximum. r/Q (W) | 394 | 477 | 
Optimum b | 0.705 | 0.92 | 
G (W) | 196.63 | 241 | 
RF peak power (kW) | 1100 |  | 
Elliptical cavities
Spoke cavities
Geometric beta | 0,50
Frequency (MHz) | 352,2
Nominal Accelerating gradient (MV/m) | 9
Lacc (bopt.x nb gaps x l/2) (m) | 0,639
Bpk (mT) | 79 (max)
Epk (MV/m) | 39 (max)
Bpk/Eacc (mT/MV/m) | <8,75
Epk/Eacc | <4,38
Beam tube diameter (mm) | 50
RF peak power (kW) | 335
G (W) | 130
Max R/Q (W) | 427
Qext | 2,85 105
Q0 at nominal gradient | 1,5 109

## Slide 6: ESS Linac Layout
Target
A2T  DgLg  HEBT
(56 m)
571 MeV
Cryo
Spoke
Medium β
(77 m)
(179 m)
High β
2000 MeV
216 MeV
75 keV
Warm
Source
DTL
MEBT
RFQ
LEBT
(2.4 m)
(4.6 m)
3.6 MeV
(3.8 m)
(39 m)
90 MeV
 | Num. of CMs | Num. of cavities
Spoke | 13 | 26
Medium b (6-cell) | 9 | 36
High b (5-cell) | 21 | 84
Beam power (MW) | 5
Beam current (mA) | 62.5
Linac energy (GeV) | 2
Beam pulse length (ms) | 2.86
Repetition rate (Hz) | 14

## Slide 7: Cryomodules Function
A Cryomodule permits to operate SRF cavities in a cryogenics atmosphere.
For ESS, the Spoke and Elliptical cavities operate in a saturated superfluid helium bath

## Slide 8: Environment - Superfluidity Helium and Supraconductivity (see Steve Molloy’s presentation)
Normal-fluid fraction:
excited states atom (phonons & rotons)
 like a conventional viscous fluid
finite density , rn
finite viscosity, 
entropy, s
Superfluid fraction:
- atoms that have undergone BEC
 like an ideal inviscid liquid resulting in the absence of classical turbulence.
finite density, rs
NO viscosity
carry NO entropy
irrotational behavior for an inviscid fluid
but vortices can be generated in the superfluid component
Quantized vortices
Counter-flow turbulence
Helium (25 %) is the most common element in Universe after Hydrogen (73 %)
Two isotopes: 3He (fermion) & 4He (boson)
Macroscopic quantum physic system simplification
The two-fluid model is only a phenomenological model !
No bulk flow
Heat flux
Counter-flow mechanics

## Slide 9: Spoke cryomodule
Thermal shield
T° -200°C
Supports
A cryomodule: what is it and what for?
Thermal conduction
RF electro magnetic wave (352 MHz)
Superconducting radiofrequency (SRF) cavity
T°-269°C
Thermal radiation
Room T°
Vacuum
Vacuum
1/ To provide a cryogenic environment to the cold mass (cavity) = cryostat:
- distributing the cryofluids to cool-down and maintain at cold T° (LHe, LN2)
- limiting the heat transfers
Vessel
Acknowledgment: Patxi Duthil

## Slide 10: Spoke cryomodule
A cryomodule: what is it and what for?
Supports
Vacuum vessel
2/ To support the cavities and perform accurate alignment
- with respect to the beam axis
- with respect to other linac components (cryomodules, diagnostics, tunnel)
NB: alignment must be preserved during thermal and pressure cycles
Supports
Tunnel
Cryomodule
Diag

## Slide 11: Spoke cryomodule
A cryomodule: what is it and what for?
Vacuum vessel
3/ To offer magnetic shielding
- from the local magnetic sources
- from the earth magnetic shield
NB: the magnetic shield might be cooled (for better performances)
Magnetic shield

## Slide 12: Spoke cryomodule
A cryomodule: what is it and what for?
Vacuum vessel
4/ To provide all interfaces between the cavity and the tunnel:
- beam pipe
- RF
- cryogenic
- vacuum
- diagnostic (instrumentation)
- mechanical (support and alignment)

## Slide 13: Outline
  Cryomodule Functions
  Cryomodule Components
  Cryomodule Assembly
  How to operate a cryomodule

## Slide 14: ESS SRF cavities and cryomodules
4 Elliptical Cavities per Cryomodule
2 Spoke Cavities per Cryomodule
Power coupler
Cold tuning System
Nb cavity enclosed in Ti Helium tank
Segmented SRF linac with RT focusing elements
Magnetic shield
Notes: 2 spoke – 3 gap
4 cavity – SNS like
Segmented SRF linac with RT focusing elements

## Slide 15: Spoke cryomodule
Diameter
1350 mm
2900 mm

## Slide 16: Elliptical cryomodule
Similar to CEBAF/SNS cryomodule concept with 4 cavities per cryomodule
Common design for medium (6 cells) and high beta (5 cells) cavities
Proton Beam
Jumper connection
Magnetic shielding
Power coupler
Cavity with Helium tank
Diphasic He pipe
Thermal shielding
Regulation He valve
Intercavities bellows
Vacuum valve
Spaceframe support
Heat exchanger
Alignment fiducial
Warm to cold transition

## Slide 17
Access traps to the tuners
Elliptical Cryomodule Components
The cryomodule design and calculation:
Thermo-mechanical studies
Magnetic studies
Safety analysis to size all components
Reliability analysis, FMEA
50K Thermal shield
Lateral port
(CTS, alignment)
Tie rods (TA6V)
Positioning jacks
(3 at 120°)
Power coupler
Wave-guide transition
Guide rail and wheel
Space frame
Vacuum vessel
(stainless steel - 1200 mm diam.)
Two phase He pipe
Positioning optical devices
Cryogenic line interface

## Slide 18: Thermal shield for Spoke cryomodule
    Material: Al6062
    Thickness: 2 mm
He 20 bars
(machine)
Sat N2
(Proto)
    Assembled and supported (rods)

## Slide 19: Safety relief devices
Identify: Hydraulic circuits
  volume and pressure
    fluid
  most credible incident
Assess/calculate:
Pressure drop distribution
        Mass-flow to extract
        Diameter of the relief
        Type of device
Mitigate/design 

## Slide 20: Cavity package
Doorknob – Transition between
the coaxial power coupler and
the WR2300 rectangular waveguide
Cold Tuning System
Heat exchanger necessary to make
the transition from 300 K to 2 K
Integrating a mechanical system
to compensate efforts
RF Power Coupler
Double Spoke Cavity

## Slide 21: Cold Tuning System
2 piezo stacks
Stepper motor and planetary gearbox (1/100e) at cold and in vacuum
Slow tuner
Main purpose : Compensation of large frequency shifts with a low speed
Actuator used : Stepper motor
Fast tuner
Main purpose : Compensation of small frequency shifts with a high speed
Actuator used : Piezoelectric actuators
Type V ; 5-cell prototype
+/- 3 mm range on cavity
Elliptical CTS
Spoke CTS
&

## Slide 22: Cavities tuning: Lorentz De-tuning
Because of the enormous gradients in superconducting cavities,
  the radiation pressure deforms the cavities
We expect over 400 Hz of detuning in the ESS cavities
  Unloaded cavity bandwidth = 0.07 Hz
  Loaded cavity bandwidth = 1 kHz
The mechanical time constant of the cavities is about 1 ms compared to the pulse length of 3 ms
  Static pre-detuning as done in SNS will not be sufficient
  Dynamic de-tuning compensation using piezo-electric tuners is a must!
  Or else pay for the extra RF power required
ESS and long pulse: 2.86 ms

## Slide 23: The Spokes Cryomodule
4 HPR Ports
Coupler port
Bellows
Helium tank

## Slide 24: Fundamental Power Coupler
Antenna
Vacuum
Outer conductor
(LHe-cooled)
Doorknob
Inner conductor
(water-cooled)
Al2O3
ceramic disc
RF input
Short circuit
WR2300
Elliptical:
1.1 MW
Spoke:
335 kW

## Slide 25: Magnetic shield for Elliptical Cavity
Limit contribution of the trapped flux to the surface resistance to 4 nW
Limit the external static field to Bext = 14 mG.
→ Required shielding efficiency equal to 35.
Achievable with 1.5 mm,
µr =20000 shielding material
Courtesy of J. Plouin/ CEA

## Slide 26: Magnetic shield for Spoke Cavity
Tuner side ends
Cavity bellow side ends
External shield
Coupler shield
Internal shield
Cooling circuit
Shield support
Shrim
Material: Cryophy®
Actively cooled (better performances)
    Magnetic shields fabricated
    Assembly test performed
    To be tested within the cryomodule

## Slide 27: Validation of spoke cryomodule component performance
Step 1: Spoke cavity
@ IPNO
@ Uppsala University - HNOSS
Step 3: Cryomodule w/ prototype valve box
@ IPNO
@ UU - HNOSS
Double spoke cavity, 352.2 MHz, b=0.50
Goal: Eacc = 9 MV/m [Bp= 62 mT; Ep = 39 MV/m]
Lorentz detuning coeff.: ~-5.5Hz/(MV/m)2
Tuning sensitivity Df/Dz = 130 kHz/mm
Step 2: Spoke cavity packages
@ IPNO - Warm and 4 K
@ UU - HNOSS
Notes: between coaxial power coupler and WR2300 waveguide
(eg. mag. Shield cooling validated at HNOSS !)

## Slide 28: Spoke cavities results @ IPNO
Romea
Giulietta
Germaine
View of the spoke cavity bars
Magnetic shield
Spoke cryomodule vacuum vessel:
Fabrication achieved (FAT done)
Inter-cavity bellows
Thermal shield
Cold Tuning System
Chart: Eacc (MV/m)
| 1.0411528408 | 1.3636863344 | 1.7960337294 | 2.3785620664 | 3.1616550763 | 4.2512288902 | 5.691994718299967 | 7.607894620699959 | 9.2889042977 | 10.4909420585 | 11.4872080919 | 11.9857299507 | 12.4685080044 | 12.8918275788 | 13.3249162609 | 8.5175460142 | 6.779762624 | 10.4511598048 | 10.9336329049 | 12.4269482109 | 12.6477854083 | 12.8547752644 | 5.4158233259 | 4.8190839113 | 6.086456023099998 | 8.9797550147 | 9.3468331122 | 9.5019882365 | 10.0176184989 | 10.530875743 | 11.0170288936 | 12.4900589582 | 12.7047021662 | 12.9155970886 | 12.8933118907 | 7.8499065817 | 7.1798354067 | 6.404931485999999 | 3.3908961438 | 3.6835323509 | 0.4931902569189 | 0.4095571275839 | 0.3096096499948 | 12.6638129862 | 12.8769938544
February 2016 (2K) with no baking nor heat treatment | 24811813972.8 | 25055512686.8262 | 24904745595.0754 | 24149592102.5771 | 23544677975.847 | 21282355957.2568 | 19022438411.9148 | 15440267258.7082 | 10532305345.458 | 9751812018.7519 | 8017640926.9093 | 7201092570.6186 | 6453453066.5486 | 5789272712.0284 | 5147451417.7115 | 13052028240.0197 | 16057237942.365 | 9478477664.7803 | 8666466595.7421 | 6345232495.7639 | 6010228842.6951 | 5706283270.2295 | 18678214923.9497 | 19710215363.5366 | 17770509373.7967 | 12604010022.4852 | 10710666314.7803 | 11889546745.8404 | 10841777626.341 | 9873317080.2164 | 9016995015.7115 | 6428297484.6623 | 5462319196.3891 | 5110792713.0535 | 5131125434.4896 | 14477346579.471 | 15524401516.623 | 16949626923.9104 | 22181949463.4208 | 21371357887.1672 | 25640907805.8863 | 24098906292.1639 | 25940359889.2546 | 5481189119.106 | 5111372856.177
January 2017, 1st cool down (2K): no baking, heat treatment @ 650°C, 10h | 34619624096.5 | 36237937303.6 | 34979034647.5 | 34799839790.9 | 34197007849.7 | 34181267261.3 | 32631941359.2 | 29718831689.2 | 30992582664.4 | 16161750592.8 | 19132609346.5 | 21972966321.1 | 16886693176.3 | 12039735448.9 | 33768083768 | 29688980455 | 27543949176.7 | 23703000002.5 | 17938590398.3 | 12620172295.6 | 13107051344.5 | 13020265298.6 | 25402381413.8 | 19134426282.5 | 13145977206.8
January 2017, 2nd cool down (1.7 K) | 44320818435.6 | 45092759760.7 | 45810555355.1 | 43845957154.3 | 45448231392.7 | 44673028767.8 | 45066011213.5 | 45609976605.4 | 44549938133.2 | 43668717721.7 | 42592423594.2 | 39398555072.8 | 32976814104.5 | 27812752442.5 | 27443386256.6 | 22232097233.4 | 15124353433.5 | 9154505046.9 | 37041983192
Cavity losses=2W (4% d.c.) | 4792531.3192 | 19170125.2768 | 43132781.8727 | 76680501.1071 | 119813282.9798 | 172531127.4909 | 234834034.6404 | 306722004.4283 | 388195036.8546 | 479253131.9192 | 579896289.6223 | 690124509.9637 | 809937792.9435 | 939336138.5617 | 1078319546.8182 | 1226888017.7132 | 1385041551.2465 | 1552780147.4183 | 1730103806.2284 | 1917012527.6769 | 2113506311.7638 | 2319585158.489 | 2535249067.8527 | 2760498039.8547 | 2995332074.4951 | 3239751171.7739 | 3757344554.2467 | 4313278187.273 | 4907552070.8528 | 5540166204.9861 | 6211120589.673 | 6920415224.9135 | 7668050110.7075 | 8454025247.055 | 9278340633.9561
Chart: Eacc (MV/m)
| 0.5780946296218 | 0.7962490641163 | 1.0835499462 | 1.4694301106 | 1.9870048853 | 2.6881217504 | 3.663944908 | 4.960197109 | 5.9415387637 | 7.6014936122 | 6.719685307400001 | 8.5683842629 | 9.6827548155 | 10.2293711167 | 10.8454839227 | 11.4749006711 | 12.1324618645 | 12.7452669112 | 13.3751584271 | 13.9427658773 | 14.4826799998 | 14.9347836235 | 15.3549686783 | 15.3320043884
June 2015 (2K) with no baking nor heat treatment | 16716381292 | 16600648231.8 | 16382806425.2 | 16208904940.7 | 15716881826.4 | 15362303048.6 | 14449832216.6 | 13592441241.3 | 12729219704.7 | 11530651622.7 | 12166657627 | 10729767033.2 | 9837504193.3 | 9355074716.7 | 8845475825.1 | 8362663483.8 | 7880524300.2 | 7372864343.3 | 6746950901.7 | 6138095987.4 | 5472493530.9 | 4877934989.3 | 4312450072.9 | 4304828855.7
Dec 2016, 1st cool down (2K): no baking, heat treatment @ 650°C, 10h | 26074774202.7 | 27300082121.8 | 26331262624.8 | 25987500753 | 26328935445.5 | 26424964478 | 25425493420.5 | 24648171204 | 22853447074.5 | 21949961270.3 | 19618973774.3 | 15855596564 | 13758354933.2 | 11547215993.9 | 9714813555 | 9610027544.2 | 24779963068.9 | 9667795875.7 | 9494077849.4 | 9447060304.7 | 9297756211.3 | 8825949740.4 | 8738366809.5 | 15364714500.5 | 19540785980.5
Dec 2016, 2nd cool dow (1.7K) after 30h @ 100K | 36148786956.7 | 38789612499.5 | 31327673809.4 | 38785812149.5 | 38066645156.2 | 37917311562.6 | 37302034534.9 | 38050674774.1 | 30972457172.6 | 34140699876.5 | 36417655643.9 | 37393452137.3 | 37311881277.6 | 25549617832.8 | 36881160491.2
Cavity losses=2W (4% d.c.) | 4792531.3192 | 19170125.2768 | 43132781.8727 | 76680501.1071 | 119813282.9798 | 172531127.4909 | 234834034.6404 | 306722004.4283 | 388195036.8546 | 479253131.9192 | 579896289.6223 | 690124509.9637 | 809937792.9435 | 939336138.5617 | 1078319546.8182 | 1226888017.7132 | 1385041551.2465 | 1552780147.4183 | 1730103806.2284 | 1917012527.6769 | 2113506311.7638 | 2319585158.489 | 2535249067.8527 | 2760498039.8547 | 2995332074.4951 | 3239751171.7739 | 3757344554.2467 | 4313278187.273 | 4907552070.8528 | 5540166204.9861 | 6211120589.673 | 6920415224.9135 | 7668050110.7075 | 8454025247.055 | 9278340633.9561
No heat treatment
No baking
Notes: Germaine died after final BCP (after HPR)
Eacc_max=15.3 MV/m achieved with “Romea” , Qo > 1.6 1010
Several MP barriers but easily processed.
Strong FE at max gradient
Limitation is the cooling capacity (unstable conditions, cavity in vertical position)

## Slide 29: Test Stand and coupler conditioning @ IPNO
Control and security rack
(with fast interlocks)
Clean room ISO 4
Surface treatment
lab
Furnace
Vertical cryostats
Power coupler conditioning
Notes: Infrastructure adapted from earlier use (e.g. Spiral2)
Heat treatment furnace by the earlier cooperation agreement – chemical treatment
Conditioning of power-coupler

## Slide 30: Outline
  Cryomodule Functions
  Cryomodule Components
  Cryomodule Assembly
  How to operate a cryomodule

## Slide 31
Cavity fabrication
Cryomodule components fabrication
Cavity string assembling in clean room
Validation test of the cavity in vertical cryostat
Validation test of the cryomodule
Cryomodule on beam line
Power coupler fabrication
Coupler RF processing
Cryomodule assembling
Tools fabrication
Chemical treatment
High pressure rinsing
In clean room (ISO5 or ISO4)
Assembling in clean room
Transport
Qualified cavity storage
Cryomodule reception and storage
Cryomodule storage
Processed couplers storage
Space frame
Beam valves and extremity flange
TA6V rods in X pattern to keep the beam axis at the same position during cool down
Magnetic shield
Tuning system
Cryomodule life-cycle
31
Notes: QA control

## Slide 32: Elliptical Cavity Preparation
Vertical Electropolishing system@ CEA
Elliptical beta cavity fabrication

## Slide 33: Elliptical Assembly Procedure
Cavity string assembly in clean room
Cold mass assembly (outside the clean room)
Thermal shield
Spaceframe
Vacuum
vessel
Design concept of the tooling: most of parts will be used for both types of elliptical cryomodules
Build on existing knowledge (SNS, XFEL)
Develop Training and “Fabrication file”
Pre-industrialization
Industrialization
Notes: Only minor differences:
  Length of the inter-cavity bellows, details in cryo piping, beam pipe bellows
  Tuner piezo frames
  Penetration of the antenna for Qext adjustment

## Slide 34: Infrastructure in Saclay
IS0 5
52,69 m2
IS0 7 27,5 m2
Water cleaning
High Pressure Rinsing HPR
    The clean room inauguration
     May 13th 2014
    Clean room for the M-ECCTD (and H-ECCTD)
    Possible IKC for the assembly by industry at Saclay (XFEL cryomodules assembly)
    Uses the current infrastructure at Saclay
    Benefits from the experience of the XFEL cryomodule assembly (ALSYOM)
Notes: Only minor differences:
  Length of the inter-cavity bellows, details in cryo piping, beam pipe bellows
  Tuner piezo frames
  Penetration of the antenna for Qext adjustment

## Slide 35
Assembly process inside the clean room

## Slide 36: Outline
  Cryomodule Functions
  Cryomodule Components
  Cryomodule Assembly
  How to operate a cryomodule

## Slide 37: Cryomodule Interfaces
Cryogenic distridution
Disciplines: beam optics, RF, cryogenics, vacuum, electrical, cooling
Test stands
Control command (Control Box, PLC, LLRF, MPS, EPICS)
Quality Assurance
Data-logging
ES&H
Conventional Facility
Survey
Logistics (Transport, storage)
Cryogenic distribution
Radio-Frequency
Beam Vacuum
Beam Diagnostic
Beam Optics
Control system

## Slide 38
RF power test stations at CEA Saclay
704 MHz
RF Plateform
Pilot
Switch RF
Security box
water
C/C
C/C
Water
vacuum
Safety
RF
Fast acquisition (RF signals, electron pick-up,
arc detector by photomultipliers)
+ slow acquisitions (vacuum…)
Signals for fast interlock
Coupler Conditioning
Security box
C/C
C/C
C/C
Water
Vacuum
Cryo
safety
RF
ESS Cryomodule
(ECCTD+ pre-series)
Security box
C/C
Klystron:
704 MHz
1 MW
Modulator HT 110 kV
Circulator + load
waveguides
Supratech
Cryogenic system
Manual switch

## Slide 39: Test Stand @ Uppsala (FREIA)
RF Power Source + LLRF
Cryogenics
SRF cavity
Control System & Interlock
HNOSS
Spoke & Elliptical cavity package
Notes: Thanks to an earlier collaboration with UU to build up capacity in UU from 2011
support for multi-disciplinary cryostat and lab

## Slide 40: Validation of Elliptical Medium-b Technology Demonstrator
Step 1: Elliptical cavities
Medium-beta
@ Saclay
@ LASA
 | LASA | CEA
Qext | 7.7× | 7.5×
k | 1.55% | 1.22%
sep. (MHz) | 0.70 | 0.54
G (Ohm) | 198.8 | 196.6
r/Q (Ohms) | 374 | 394
Epeak/Eacc | 2.55 | 2.36
Epeak (MV/m) | 42.6 | 40
Bpeak/Eacc(mT/MV/m) | 4.95 | 4.79
 | LASA | CEA
Qext |  | 
k | 1.55% | 1.22%
sep. (MHz) | 0.70 | 0.54
G (Ohm) | 198.8 | 196.6
r/Q (Ohms) | 374 | 394
Epeak/Eacc | 2.55 | 2.36
Epeak (MV/m) | 42.6 | 40
Bpeak/Eacc(mT/MV/m) | 4.95 | 4.79
@ Saclay
@ Lund
Step 2: M-Elliptical Cavity Cryomodule Technology Demonstrator
M-ECCTD = 3 CEA cavities + 1 LASA cavity
Notes: Design of Mb (even if Hb first proto in the framework of the cooperation agreement).
Test of 6 Mb
Added LASA in the SRF collaboration at a later stage.
Complete a new RF design plug-compatible with Mb cryomodule. test
Cell to cell coupling, k
Pi and 5pi/6 separation mode +30%

## Slide 41
Process and Instrumentation Diagram
Instrumentation function
  Monitoring
  Control
  Interlock
  Alarms
Operating Modes under definition

## Slide 42: Cryogenic operating modes
Acknowledgment : N Elias

## Slide 43: Control integration

## Slide 44: Superconducting linac
 | MEDIUM-β | HIGH-β
β | 0.67 | 0.86
# CM | 9 | 21
Cav. /CM | 4 | 4
# Cav. | 36 | 84
CM L [m] | 6.584 | 6.584
Sector L [m] | 77 | 179
Proton Beam
Elliptical cavity Cryomodules ECCTD
Klystron gallery
→ 70% of the phisical length of the linac
 95 % of the proton acceleration

## Slide 45: Elliptical (704 MHz) RF System Layout
One cavity per klystron
4 klystrons per modulator
16 klystrons per tunnel penetration
Tunnel

## Slide 46: Elliptical (704 MHz) RF System Layout
4.5 Cells of 8 klystrons for Medium Beta
10,5 Cells of 8 klystrons (IOTs) for High Beta
WR1150 Distribution
Klystrons
Modulator
Racks and Controls

## Slide 47
ESS SRF Linac Collaborative Space: https://confluence.esss.lu.se/display/CRYOM
US-Particle Accelerator School, http://uspas.fnal.gov/materials/materials-table.shtml
CERN Accelerator School, http://cas.web.cern.ch/cas
JUAS, https://espace.cern.ch/juas/SitePages/Home.aspx
NPAS, https://npap.eu/
Few books
RF Linear Accelerators, T.P. Wangler, Wiley, 2008
RF Superconductivity for Accelerator, H. Padamsee, J. Knobloch, T. Hays, Wiley, 2011
An introduction to particle accelerators, E.J.N. Wilson, Oxford Univ. Press, 2001
An introduction to the physics of high-energy accelerators, D.A. Edwards & M.J. Syphers, Wiley, 1993
Acknowledgements & References

## Slide 48: Extra slides

## Slide 49: The Spokes Cryomodule
Power coupler double wall cooling
C-W transition
Cold Tuning System
2-phase manifold
Alignment tie rods
Power coupler antenna cooling
Ceramic disk, 100 mm diameter
400 kW peak power (335 kW nominal)
Antenna & window water cooling
Outer conductor cooled with SHe
Double spoke cavity (3-gaps), 352.2 MHz, b=0.50
Goal: Eacc = 9 MV/m [Bp= 62 mT ; Ep = 39 MV/m]
4.2 mm (nominal) Niobium thickness
Titanium Helium tank and stiffeners
Lorentz detuning coeff. : ~-5.5 Hz/(MV/m)2
Tuning sentivity Df/Dz = 130 kHz/mm