## Slide 1: Neutron Instruments
Ken Andersen
LTH Engineering course
7th December 2017

## Slide 2: Summary
Neutron instrument concepts
  time of flight
  Bragg’s law
Neutron Instrumentation
  guides
  detectors
  choppers
  pulse-shaping
Neutron diffractometers
Neutron spectrometers

## Slide 3: De Broglie Relations
Particle | Wave

## Slide 4: The time-of-flight (TOF) method
distance
time
Δt

## Slide 5: Diffraction: Bragg’s Law

## Slide 6: Diffraction: Bragg’s Law

## Slide 7: Diffraction: Bragg’s Law

## Slide 8: Diffraction: Bragg’s Law

## Slide 9: Diffraction: Bragg’s Law
dsinq

## Slide 10: Diffraction: Bragg’s Law
dsinq

## Slide 11: Diffraction: Bragg’s Law
dsinq
2θ

## Slide 12: Diffraction: Bragg’s Law
Wavevector:

## Slide 13: Diffraction: Bragg’s Law
Wavevector:
θ
θ

## Slide 14: Diffraction: Bragg’s Law
θ
θ
θ
θ

## Slide 15: Diffraction: Bragg’s Law
θ
θ
Bragg’s Law:

## Slide 16: Diffraction: Bragg’s Law
θ
θ

## Slide 17: Diffraction: Bragg’s Law
θ
θ
Bragg’s Law:

## Slide 18: Diffraction: Bragg’s Law
θ
θ
Bragg’s Law:
Conversion:

## Slide 19: Reflection: Snell’s Law
n=1
n’<1
incident
refracted
reflected
θ
θ’

## Slide 20: Reflection: Snell’s Law
n=1
n’<1
incident
refracted
reflected
θ
θ’
θ’=0: critical angle of total reflection θc

## Slide 21: Reflection: Snell’s Law
n=1
n’<1
incident
refracted
reflected
θ
θ’
θ’=0: critical angle of total reflection θc

## Slide 22: Reflection: Snell’s Law
n=1
n’<1
incident
refracted
reflected
θ
θ’
θ’=0: critical angle of total reflection θc
for natural Ni,
θc = λ[Å]0.1
Qc = 0.0218 Å-1

## Slide 23: Reflection: Snell’s Law
n=1
n’<1
incident
refracted
reflected
θ
θ’
θ’=0: critical angle of total reflection θc
for natural Ni,
θc = λ[Å]0.1
Qc = 0.0218 Å-1
Definition:

## Slide 24: Neutron Supermirrors
Courtesy of J. Stahn, PSI

## Slide 25: Neutron Supermirrors
Courtesy of J. Stahn, PSI

## Slide 26: Neutron Supermirrors
Courtesy of J. Stahn, PSI

## Slide 27: Neutron Supermirrors
d1
}
l 1
l 2
l 3
l 4
l c
d2
}
d3
}
d4
}
Reflection: θc(Ni) = λ[Å]  0.10
Multilayer: θc(SM) = m  λ[Å]  0.10

## Slide 28: Neutron Supermirrors
}
l 1
l 2
l 3
l 4
l c
}
}
}
Reflection: θc(Ni) = λ[Å]  0.10
Multilayer: θc(SM) = m  λ[Å]  0.10
“m-number”
Supermirror critical angle
d1
d2
d3
d4

## Slide 29: State-of-the-art Supermirrors
Mirrotron

## Slide 30: State-of-the-art Supermirrors
Mirrotron
Swiss Neutronics

## Slide 31: Neutron guides
WISH @ ISIS
Swiss Neutronics guides for NIST

## Slide 32: Distribution by Guides
Neutron Guides:
Creating space for instruments

## Slide 33: Background Reduction
Distance:
  move away from fast-neutron source ~ 1/R2
Guides can be used to reduce background

## Slide 34: Background Reduction
Distance:
  move away from fast-neutron source ~ 1/R2
Curved Guides:
  avoid direct line-of-sight
  avoid gammas
  avoid fast neutrons
Guides can be used to reduce background

## Slide 35: Focusing
Converging guide increases flux, but increases divergence
(Liouville’s theorem)
Guides can also be used to increase flux

## Slide 36: Diffractometers
Measure structures (d-spacings)
Very general method:
  crystals
  powders
  polycrystalline materials
  liquids
  large molecules or structures
  surfaces

## Slide 37: Diffractometers
Measure structures (d-spacings)
Very general method:
  crystals
  powders
  polycrystalline materials
  liquids
  large molecules or structures
  surfaces
Ideal diffractometer:
  measure ki of each incident neutron
  measure kf of the same neutrons

## Slide 38: Diffractometers
Measure structures (d-spacings)
Very general method:
  crystals
  powders
  polycrystalline materials
  liquids
  large molecules or structures
  surfaces
Ideal diffractometer:
  measure ki of each incident neutron
  measure kf of the same neutrons
No magic monitors or detectors!

## Slide 39: Diffractometers
Measure structures (d-spacings)
Very general method:
  crystals
  powders
  polycrystalline materials
  liquids
  large molecules or structures
  surfaces
Ideal diffractometer:
  measure ki of each incident neutron
  measure kf of the same neutrons
No magic monitors or detectors!
No energy-sensitive detectors!

## Slide 40: Diffractometers
Measure structures (d-spacings)
Very general method:
  crystals
  powders
  polycrystalline materials
  liquids
  large molecules or structures
  surfaces
Real diffractometer:
  measure ki or kf of the beam
    time-of-flight
    Bragg diffraction
  assume ki = kf
No magic monitors or detectors!
No energy-sensitive detectors!

## Slide 41: Powder diffractometers
Polycrystal
Measure crystal structure using Bragg’s law
  Rietveld refinement
Large single crystals are rarely available

## Slide 42: Time-of-flight (TOF) Method
distance
time
sample
detector
Δt

## Slide 43: Time-of-flight (TOF) Method
distance
time
sample
detector
Δt

## Slide 44: Time-of-flight (TOF) Method
POLARIS @ ISIS TS1

## Slide 45: Crystal Monochromators
Copper 200
Graphite 002
 | d-spacing
Germanium 333 | 1.089 Å
Copper 200 | 1.807 Å
Silicon 111 | 3.135 Å
Graphite 002 | 3.355 Å

## Slide 46: Pulsed source time structures (λ=5Å)
log(Intensity@λ=5Å)
0 20 40 80 100 120
time (ms)
1
0.1
0.01
ISIS-TS1 128kW
ISIS-TS2 32kW
100μs
0
short pulse
ILL 57MW

## Slide 47: Pulsed source time structures (λ=5Å)
log(Intensity@λ=5Å)
0 20 40 80 100 120
time (ms)
1
0.1
0.01
ISIS-TS1 128kW
ISIS-TS2 32kW
100μs
0
short pulse
ILL 57MW

## Slide 48: Constant-Wavelength Diffraction
D1B @ ILL
Rietveld refinement
2θ
Debye-Scherrer cone

## Slide 49: Diffuse Scattering: Local Structure

## Slide 50: Single Crystal Diffraction
Complex structures
  powder averaging removes information
Magnetic structures
Large unit cells
  Protein crystallography
Two approaches:
  Monochromatic/TOF instrument
  Laue diffractometer (white beam)

## Slide 51: Single Crystal Diffraction
(110)
(310)
(120)
λ(110)
λ(120)
λ(310)
Complex structures
  powder averaging removes information
Magnetic structures
Large unit cells
  Protein crystallography
Two approaches:
  Monochromatic/TOF instrument
  Laue diffractometer (white beam)

## Slide 52: Small Angle Neutron Scattering (SANS)

## Slide 53: Small-Angle Neutron Scattering
Monochromator
Δλ/λ
2θ
Q
Collimator
Detector
Sample
d
λ d 2θ
4-20 Å 5-3000 Å 0.1-20°
Probing the longest length scales available to neutrons

## Slide 54: Reflectometry
Reflection from surfaces and interfaces
in
out
Specular: θin=θout
Off-specular: θin≠θout
Log
Depth profile of the scattering-length density

## Slide 55: Reflectometry
Horizontal sample geometry
all samples (including free liquids, and liquid-liquid interfaces)
Vertical sample geometry
solid samples, e.g. magnetic
solid-liquid interfaces
straightforward to vary θ

## Slide 56: Neutron Spectroscopy
Excitations: vibrations and other motions
  lattice vibrations
  magnetic excitations
  quasi-elastic scattering: diffusion & relaxation

## Slide 57: Neutron Spectroscopy
Excitations: vibrations and other motions
  lattice vibrations
  magnetic excitations
  quasi-elastic scattering: diffusion & relaxation
Ideal spectrometer:
  measure ki of each incident neutron
  measure kf of the same neutrons

## Slide 58: Neutron Spectroscopy
Excitations: vibrations and other motions
  lattice vibrations
  magnetic excitations
  quasi-elastic scattering: diffusion & relaxation
Real spectrometer:
  measure ki and kf of the beam
    time-of-flight
    Bragg diffraction
  Fix ki and scan through kf – “direct geometry”
  Fix kf and scan through ki – “indirect geometry”

## Slide 59: Chopper Spectrometers
distance
time
chopper
detector
sample
0
Direct geometry:
fix ki by chopper phasing
scan through kf by time-of-flight

## Slide 60: Neutron Choppers
Disk choppers
Fermi choppers
f < 300 Hz
Δt > 10μs
f < 600 Hz
Δt > 1μs

## Slide 61: Chopper Spectrometers
General-Purpose Spectrometers
    Incident energy ranges from 1meV to 1eV
Huge position-sensitive detector arrays
    Single-crystal samples

## Slide 62: Detectors
3He gas tubes
n + 3He  3H + 1H + 0.764 MeV
>1mm resolution
High efficiency
Low gamma-sensitivity
3He supply problem
Scintillators
n + 6Li  4He + 3H + 4.79 MeV
<1mm resolution
Medium efficiency
Some gamma-sensitivity
Magnetic-field sensitivity

## Slide 63: Detectors
10B detectors
n + 10B  7Li + 4He + 0.48 MeV
massive development programme
none yet in operation
many different types
inclined blades
perpendicular blades
boron layer thickness limited to ~ 1 μm
=> ~ 5% efficiency

## Slide 64: Alternative to Direct Geometry
distance
time
detector
sample
0
Indirect geometry:
fix kf – usually by analyser crystals
scan through ki by time-of-flight
analyser

## Slide 65: Vibrational Spectroscopy
TOSCA@ISIS
Density-of-states measurements

## Slide 66: Backscattering
BASIS@SNS Si111 3μeV
OSIRIS@ISIS PG002 25μeV

## Slide 67: Triple-Axis Spectrometers
Single-crystal excitations
Very flexible
Measures a single point in -E space at a time
Scans:
    Constant : Scan E at constant ki or kf
    Constant E: Scan in any direction

## Slide 68: Neutron Imaging
Neutrons
X-rays

## Slide 69: Summary
Neutron Instrumentation
  guides
  detectors
  choppers
Neutron diffractometers
  powder diffraction
  single-crystal diffraction
  SANS
  reflectometry
Neutron spectrometers
  direct-geometry time-of-flight
  backscattering
  triple-axis
Imaging

## Slide 70
10-14
10-11
10-9
10-7
10-2
10-1
Time [s]
10-12
10-9
10-15
10-6
10-3
1
103
10-6
Particle Physics
Spin-echo
Imaging
Reflectometry
10-10
10-12
10-15
10-8
10-5
Visible Light
Infrared
Light
FTIR
Raman
Brillouin
Dynamic Light Scattering
Laser PCS
10-6
Inelastic X-ray Scattering
hydrogen modes
lattice vibrations
spin dynamics
rotational tunneling
molecular diffusion
dynamics of macromolecules
domain wall dynamics
NMR
mSR
Dielectric Spec.
Backscattering
UV & X-ray FEL: Pump & Probe studies
texture
industrial components
bacteria
cell membranes
magnetic structures
atomic structures
viruses
magnetic domains
polymers, proteins
charge density
NMR Imaging
Triangulation
NMR
X-ray Imaging
SAXS, X-ray Refl.
X-ray Diffraction
EXAFS & XANES
Microscopy
Optical Microscopy
Scanning Techniques
SNOM
AFM
STM
TOF & Crystal
Spectroscopy
Infra-red
SANS
Diffraction
elementary particles
Energy [meV]
Length [m]
102
10-1
1
10-3
101
10-2
103
X-ray Spec.
X-ray PCS
Wavevector Q [Å-1]
10-3
X-rays
NMR
Optical Nanoscopy
Electron Microscopy

## Slide 71: Thank you!
5th June 2015