## Slide 1
Carina Höglund Linda Robinson Chung Chuan Lai Per-Olof Svensson
Detector Group, European Spallation Source ERIC
carina.hoglund@esss.se
Updates from the ESS Detector Coatings Workshop in Linköping

## Slide 2
From Samson to Chewbacca
10B4C
Si
1 mm
Agrees with simulations
First prototype
(100 blades)
2014: IN5 segment (27000 blades)
2011: 2m long demonstrator
(1200 blades)
2010: First tests in Samson
2014:
Chewbacca
Process shown to be mature enough for upscaling

## Slide 3: Upscaling 2014-2017
LiU
”ESS”
3
First steps towards full production  good experience  Move 2017

## Slide 4
New coating facility
ESS facility near Linköping University
Moved March 2017
Industrial thinking and production line for ESS needs until 2025

## Slide 5
Industrial production

## Slide 6
The coating workshop
Cleaning
Mounting
Packing
Preparing
Modifying
Quality check

## Slide 7
∅ 64 cm
∅ 13 cm
About Chewbacca
Chewbacca:
CemeCon CC800/9 batch loading system
DC magnetron sputtering
Up to four 10B4C targets (50 cm height)
1-, 2-, 3-fold rotation
∅ 2-5 cm

## Slide 8
3-fold rotation (2 depositions per day):
Multigrid: 480 blades/batch  960 blades/day (IN5)  3.9 m2 coating/day ~38 cm height  Uniformity  10%
CSPEC: 330 blades/batch  660 blades/day  5 m2 coating/day
~46 cm height  Uniformity  15-20%  ~3000 m2/year are possible
2-fold rotation (3 depositions per day):
10 x 45 cm2: 10 samples/batch  30 samples/day
 2.7 m2 coating/day ~45 cm height  Uniformity  15%
Coating capacity

## Slide 9
Wrapping  1-side coated  ~50 x 200 cm2
Flat plates  2-side coated  ~60 x 60 cm2 1-side coated  ~35 x 35 cm2 x 3
Large area substrates (in a batch loading system)
Thickness heat map

## Slide 10
Collaborators since 2014

## Slide 11

10B4C coating (detector) requirements:
High quality 10B4C coatings
and
Industrial scale production
and
Cheaper than pre-2009 3He price
and
Neutron detection efficiency as good as 3He
Notes: Thin film requirement

## Slide 12
Prototype examples
MG
He-tubes
MultiGrid
MultiBlade
BandGEM

## Slide 13
Collaborators challenge us!
Coating on temperature sensitive substrates
No substrate bending when 1-side coated
Coat inside frames without bending
Cleaning of substrates to be coated
13

## Slide 14
Sometimes we fail…
14
Melting
Expanding
Bending
Dirtiness
Overheating
Wrinkling
Flaking
Flaking

## Slide 15
Advanced diagnostics techniques
Scalable
industrial production
processes
Our thin film toolbox
Materials theory
Various deposition techniques

## Slide 16
What we can provide
High quality 10B4C coatings for neutron detector applications
  Minimized residual stress
  Radiation hard
Substrates like Al, SS, Si, Al2O3, Ni, Cu, glass, etc
  ~80 at.% 10B
  Substrates like FR4, G10, Kapton, Teflon, sandwich structures, etc
  Low temperature 10B4C deposition
Flat substrates even though 1-side coated
  Coatings inside frames with ~80 at.% 10B
10B4C depositions with tailored resistivity

## Slide 17
Thank you for your attention!
carina.hoglund@esss.se

## Slide 18
High quality 10B4C coatings with DC magnetron sputtering
10B4C
Si
1 mm
Required property | Result | OK?
Good adhesion | > 1 mm on Al, Si, Al2O3, etc | 
Low residual stress | 0.09 GPa at 1 mm 10B4C on Si | 
High density | 2.45 g/cm3, 97% of bulk | 
High 10B content | 79.3 at.% of 10B | 
C. Höglund et al., J. Appl. Phys. 111, 104908 (2012)
Patent SE 535 805 C2 EU patent applications ongoing
Amount of impurities
Notes: Coatings materials properties

## Slide 19
Neutron radiation hardness (collaboration LiU-ESS-FRM II)
As-deposited
1014 n/cm2
As-deposited
1014 neutrons/cm2
 No influence on adhesion, composition, morphology, structure, etc
0.000156 % of the 10B atoms were consumed
Lifetime of 10B atoms with 108 n/cm2/s is >20 000 years 
C. Höglund et al., Rad. Phys. Chem. 113, 14 (2015)
Notes: Radiation hardness

## Slide 20
HT: High pressure, higher residual stress  Applied HT process optimal
LT: High pressure, lower residual stress  Good adhesion at LT
Schmidt, Höglund et al., J. Mater. Sci 51, 10418 (2016)
DCMS vs. HiPIMS
For low temperature?
20